## Slide 1: Structural Steel Design
Disclaimer
by Rafael Sabelli, S.E.
Notes: Graphic shows cover of NEHRP document.

## Slide 2: Chapter 9: Structural Steel Design
Steel Structures - 2
Part 1: Background/Theoretical

## Slide 3: STRUCTURAL STEEL DESIGN
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Braced frames
Other topics
Summary
Notes: Table of contents. Note that most of the substance, except the first two items, is taken from the AISC 341 Seismic Provisions for Steel Buildings, which is referenced by the Standard.
Some of the examples in this topic draw heavily on the FEMA 1051 Design Examples CD. Please see this CD for additional details.

## Slide 4: Steel Design: Context in Provisions
Design basis: Strength limit state
Using the 2015 NEHRP Recommended Provisions, Refer to ASCE 7 2016:
  Chap. 11: Seismic Design Criteria
  Chap. 12: Seismic Design Requirements (Buildings)
  Chap. 13: Nonstructural components
  Chap. 14: Design of steel structures
    Refers to AISC Specification (AISC 360-16)
    Refers to AISC Seismic (AISC 341-16)
Notes: The Provisions requirements affect design loads, limit states, and specific details required for members and connections. The bulk of the detailing rules are in the reference documents; the BSSC steel technical committee and the AISC seismic committee have been structured to work very closely together; thus, BSSC’s recommendations are incorporated into AISC Seismic very quickly.

## Slide 5: Seismic Resisting Systems
Unbraced Frames
Connections are:
  Fully Restrained Moment-resisting
  Partially Restrained Moment-resisting
Seismic classes are:
  Special Moment Frames
  Intermediate Moment Frames
  Ordinary Moment Frames
  Systems not specifically detailed for seismic response
Braced Frames
Ordinary Concentric Braced Frames
Special Concentric Braced Frames
Eccentrically Braced Frames
Buckling Restrained Braced Frames
Special Plate Shear Walls
Systems not specifically detailed for seismic response
Notes: Graphic shows frame elevations: gable frame; 10-story moment frame; 4-story eccentrically braced frame; 10-story concentrically braced frame.
Unbraced ("moment resisting") frames resist lateral forces through flexural actions of members framing into (fully or partially) rigidly connected joints. Concentrically braced frames (no moment resisting connections) resist lateral forces through truss action that causes axial forces in members. Eccentric bracing creates high moments and shears in short links intended to yield first. Overall structural deformation in tall buildings: "shear building" pattern for unbraced frame but flexural pattern in braced frame.

## Slide 6: Monotonic Stress-Strain Behavior
Notes: Graphic shows steel stress-strain curve with marked yield point and inelastic range.
Stress-strain diagram for mild steel. Note the elastic range, yield point, plastic range, and region of strain hardening. Define ductility ratio; note values of 100 or more. Compare high- and low-strength steels.

## Slide 7: Bending of Steel Beam
Strain
Stress
y <  < sh
y
y
y
sh
Section near “plastic”
Strain slightly above yield strain
Extreme fiber reaches
yield strain and stress
M
Notes: Graphic shows stress and strain diagrams for increasing moment in a beam. Strain increases with moment, but maximum stress is limited by steel yielding.
For the elastic-plastic model, regardless of strain increases at extreme fibers, stress never exceeds yield stress. However, more material yields as strain increases; stress distribution becomes partially plastic. Note that the strain diagram near plastic is prior to the onset of strain hardening.

## Slide 8: Plastic Hinge Formation
Plastic hinge in beam
Notes: Graphic shows beam-to-column connection test specimen after flexural test. Yielding of flanges and web is visible as the whitewash has flaked off.
From Modern Steel Construction – Photograph formation of a plastic hinge in a laboratory test of a RBS (reduced beam section) specimen. Yielding may be observed from flaking of whitewash from surface of steel. Very distinctive flange buckling is also visible.

## Slide 9: Cross - Section Ductility
M
Mp
My
Moment-Curvature Diagram
Notes: Graphic shows moment-curvature diagram, with curvature increasing but moment limited by flexural capacity of the beam (Mp). The yield moment is also marked.
Moment-curvature diagram shows definitions for various curvatures. Yield curvature: at first yield (at My). As moment approaches Mp, curvature increases rapidly. At Mp, curvature increases without additional moment. Ultimate curvature: curvature at failure. Behavior often idealized by extending elastic and plastic portions of curve to intersection. Note that strain hardening is not reflected in the plot.

## Slide 10: Behavior Modes For Beams
Moment
Deflection
Mp
Mr
O
M
L
A
I
G
D
J
F
B
C
E
K
H
elastic LTB
inelastic LTB
strain hardening
idealized behavior
Notes: Graphic shows moment-deflection diagram for beams with different governing limit states: lateral-torsional buckling (elastic and inelastic) and flexural yielding with strain hardening. Flexural yielding maintains high flexural strength over a relatively long range of deformation.
Note the various possible limit states (as on slide).
Strain hardening behavior is typical if hinge occurs in a region of significant shear (moment diagram is not constant). This is the typical situation, whereas the constant moment diagram in previous slide is really a laboratory idealization. Mr is the yield moment that includes the effects of residual stress.

## Slide 11: Flexural Ductility of Steel Members - Practical Limits
Lateral torsional buckling
  Provide sufficient lateral or torsional bracing
Local buckling
  Limit width-to-thickness ratios for compression elements
Fracture
  Avoid by proper detailing to allow inelastic strain
Notes: Recall from prior lesson (inelastic behavior) that structural ductility < section ductility < material ductility. Structural ductility of steel members further limited, as noted on slide, by local and lateral torsional buckling.

## Slide 12: Local and Lateral Buckling
Notes: Photograph on the left is a laboratory test of a moment end-plate connection test exhibiting local buckling. Photo courtesy of Professor T. M. Murray, Virginia Tech. Photo on right illustrates lateral torsional buckling of a cold-formed steel hat section test specimen.

## Slide 13: Lateral Torsional Buckling
L
u
f
0
Me
My
Mp
D
C
B
A
E
Laterally unbraced length
Resisting moment
inelastic buckling
elastic buckling
buckling with
strain-hardening
Notes: Graphic shows moment capacity versus unbraced length. In the low unbraced length region the moment capacity is high and is governed by flexural yielding followed by local buckling with strain hardening. It decreases with increasing length, governed by inelastic later-atorsional buckling, then by elastic LTB.
Effect of lateral-torsional buckling on moment capacity. Diagram for uniform bending of simple beam. Capacity above Mp due to strain hardening.

## Slide 14: Local Buckling
Substituting  = 0.3 and rearranging:
Classical plate buckling solution:
b
t
Notes: Graphic shows a wide-flange shape with flange half-width b and thickness t denoted.
Example correlates width-to-thickness limits for compression flanges with ductility ratios. The mathematical derivation is not truly correct because linear mechanics are extrapolated beyond the yield level by using strain as a substitute for stress. The point is to show that stability depends on width-to-thickness ratios and that high strains require stubby elements.

## Slide 15: Local Buckling continued…
This is the slenderness requirement given in the AISC specification for compact flanges of I-shaped sections in bending. The coefficient is further reduced for sections to be used in seismic applications in the AISC Seismic specification
With the plate buckling coefficient, K, taken as 0.7 and an adjustment for residual stresses, the expression for b/t becomes:
Notes: Note that AISC limits are for members expected to undergo significant inelastic deformation in a seismic event. The limits for plastic design are more liberal. These limits correspond very roughly to ductility ratio of about 10. Also note that several sections do not satisfy the limit for grade 50 steel.

## Slide 16: Width-thickness ratios
M
q
Mp
Increasing compactness
(decreasing element slenderness)
Slender elements
Elastic local buckling
Noncompact elements
Inelastic local buckling
Compact elements
Yielding
Highly compact elements
Significant strain
Notes: Graphic shows moment-rotation relationships for cross sections of different compactness. Slender elements achieve low rotation before losing strength. Flexural strength and rotation capacity increase with compactness. Both compact and highly compact sections achieve the full flexural strength, but the more compact shapes undergo greater rotation before losing strength.

## Slide 17: Restraint
Example:
Beam flange to (thick) column flange T joint
Highly restrained
Notes: Graphic shows a diagram of a T joint with a CJP weld, and a photograph of a beam-flange-to-column-flange welded joint.
Highly restrained conditions do not allow strain transverse to the direction of loading. Thus transverse stress occurs as the result of Poisson’s effect, and the steel material may not yield. Rather, the stress may continue to increase and rupture may occur at very low strain.

## Slide 18: Toughness and energy absorption
  Ductile yielding (or even achieving full strength) can be precluded by failure of low-toughness material
Minimum toughness is required for seismic design at critical locations
X
Displacement
Load
Low toughness
High toughness
X
Notes: Graphic shows a load-displacement diagram for both low-toughness and high-toughness material. The low-toughness material ruptures at a low displacement. The high-toughness material achieves larger displacement and inelastic displacement.

## Slide 19: The “k region”
Welds to this region are proscribed in seismic design
Rotary straightening of flanges strain-ages this area of the web, leading to reduced toughness.
Welds in this area have led to fracture during fabrication.
Notes: Graphic shows the K region of the beam web inside of the radiused fillet web-to-flange transition.

## Slide 20: The “k region”
“k” region
~1”-1½”
Toe of fillet
“k” dimension
Top of flange
Notes: Graphic shows the K region of the beam web inside of the radiused fillet web-to-flange transition with the k dimension denoted and the K-region indicated to be 1.5” inside of the toe of the fillet.

## Slide 21: Variability and predictability
Liu et al.
Specified minimum yield
Measured yield
Notes: Graphic shows yield strength of multiple test specimens graphed as a function of their b/t ratios. The graph shows substantial scatter, with generally higher strength for lower b/t.

## Slide 22: Expected strength
RyFy
Expected (mean) yield strength for material
NOT maximum yield strength
Determined by AISC using industry-wide data

## Slide 23: Welded Beam to Column Laboratory Test - 1960s
Notes: Graphic shows beam-to-column connection diagram with welded top and bottom plates, and moment-displacement diagram with the hysteresis somewhat similar to a parallelogram, but with a curved transition from elastic to yielding.
Load-deflection diagram for repeated reversed loads on welded joints performed under laboratory conditions in late 1960s and early 1970s. It shows relative stability of connection and its large capacity to absorb energy. Tests of joints with welded flanges and bolted webs showed similar stability and essentially same capacity. Northridge earthquake and subsequent laboratory testing have shown serious problems with particular welded joints. It turns out that it is somewhat difficult to actually achieve the behavior represented on this diagram.

## Slide 24: Bolted Beam to Column Laboratory Test - 1960s
Notes: Graphic shows beam-to-column connection diagram with bolted top and bottom plates, and moment-displacement diagram with the hysteresis with a pinched region in the center and increasing stiffness at larger displacement.
Note mildly pinched hysteresis from slipping of bolts in holes.

## Slide 25: Pre-Northridge Standard
Notes: Graphic shows beam-to-column connection diagram with welded top and bottom flanges and a bolted single-plate connection at the web. Notes indicate the column to be stronger than the beam in flexure, and continuity plates if required. Backing is shown at flange welds.
The Northridge earthquake revealed serious flaws in the performance of welded joints in steel moment frames. The drawing illustrates the particular detail that had received prescriptive acceptance for seismic-resistant design in the decade prior to Northridge. The only real variable was the weld from the shear tab to the beam web, which was required in beams in which the web represented more than 30% of the plastic flexural capacity.

## Slide 26: Backing
Backing used to support and retain molten filler metal
Backing – also called “weld backing,” “backing bars,” “back-up bars”, and “backing strips”
Fusible backing– weld is intended to bond to backing (e.g. steel backing)
Non-fusible backing– weld not intended to bond to backing (e.g. ceramic and copper)
Notes: Graphic shows detail of steel backing at a complete joint penetration groove weld with multiple weld passes.

## Slide 27: Northridge Failure
Column
flange
Backup bar
Beam flange
and web
Notes: The photo shows a cut and polished specimen with a crack at the fusion line between the weld and the column flange. Note that the backup bar is not attached to the column flange, which creates a notch normal to the stress in the flange. The section is cut at the centerline of the beam; thus, the beam web beyond the weld access hole appears as the upward curving line at the right. Note that at the instant the beam flange is in tension due to lateral sway, the column flange at the weld is also likely to be in tension.

## Slide 28: Northridge Failure
Following the 1994 Northridge earthquake, numerous failures of steel beam-to-column moment connections were identified. This led to a multiyear, multimillion dollar FEMA-funded problem-focused study undertaken by the SAC Joint Venture. The failures caused a fundamental rethinking of the design of seismic resistant steel moment connections.
Notes: The photograph shows a fracture resulting in a divot being removed from the column flange adjacent to the toe of the full penetration weld at the beam flange.

## Slide 29: Bottom Flange Weld Fracture Propagating Through Column Flange and Web
Notes: Graphic shows photo of column with fractured flange and web. The fracture line appears to go through one flange near the beam weld and entirely through the web.
Many of the buildings that experienced failures similar to that shown in the slide exhibited very little obvious signs of distress.

## Slide 30: Beam Bottom Flange Weld Fracture Causing a Column Divot Fracture
Notes: Photo showing crack in column flange at beam flange weld location. Note that the beam web and the weld access hole for the beam appear at the right side of the photo. A large divot of column-flange steel has pulled out.

## Slide 31: Northridge Failure
Bottom flange
of beam
Beam
web
Crack through weld
Note backup bar and runoff tab
Notes: The photo is a closeup view of the weld between the bottom flange of a beam and the flange of a column. Note the crack between the weld and the column flange. Also note the backup bar and the runoff tab (the diagonal bar) at the left edge of the beam flange. (The joint had been covered with spray-on fireproofing.) A fracrure in the weld at the face of the column is visible.

## Slide 32: Northridge Failures
Lamellar Tear
Heat Affected Zone
Column Flange
Column Divot
Weld Fusion
Weld
Notes: Graphics: 6 diagrams show fractures at beam bottom-flange to column-flange welded joints.
Weld: fracture is through weld material.
Weld fusion: Fracture is at weld-column boundary.
Column divot: fracture is within column flange, going from the bottom of the weld and above the joint.
Column flange: fracture is across column flange.
Heat affected zone: fracture is across beam flange.
Lamellar tear: fracture is within column flange, but extending above and below the joint.
The figures are abstracted from Interim Guidelines: Evaluation, Repair, Modification and Design of Welded Steel Moment Frame Structures, the early SAC report (95-02) on the problems found at Northridge. It is also available as FEMA 267, August 1995. The majority of the cracks began at the root of the weld directly above the notch at the end of the backup bar. Subsequent investigation determined that significant cracks exist in such joints that have not been exposed to seismic ground motion -- due to a combination of restraint of weld shrinkage, a ready-made notch, use of materials that are not “notch tough,” difficulties in inspection at the point in question, and other factors.

## Slide 33: Flexural Mechanics at a Joint
1
2
1
2
Beam Moment
Fw
Fy
2
1
1
2
Cross Sections
Fw
Fy
Notes: Graphics show:
Beam-column frame with beam section at column face (1) and slightly further from column face (2).
Bema moment diagram with high moment at section 1 and lower at section 2.
Cross section 1 is only the flanges; cross section 2 is the full wide-flange shape.
Section 1 has high stress at flanges. Section 2 has stress distribution across entire section, with yielding at the flanges.
One of the inherent weaknesses of the joint is that the flange welds must be strong enough to develop substantial yielding in the beam away from the flange in order to dissipate significant energy. The plastic section modulus is less at the welds and the gradient in the moment as one moves away from the column flange both combine to require that the ultimate strength of the weld be substantially more than the yield of the beam. Another factor is that most available beams now have yield strengths of about 50 ksi (even though sold under A36 specification) whereas the tests done at the time the joint was developed were made on material much closer to 36 ksi yield; the strength of weld metal has not changed in the same fashion.

## Slide 34: Welded Steel Frames
Northridge showed serious flaws. Problems correlated with:
  - Weld material, detail concept and workmanship
  Beam yield strength and size
  Panel zone yield
Repairs and new design
  Move yield away from column face (cover plates, haunches, reduced beam section)
  - Verify through tests
SAC Project: FEMA Publications 350 through 354
AISC 358
Notes: The slide summarizes the major points learned in the first phase of the SAC project (a FEMA-funded joint venture of SEAOC, ATC, and CUREE, which is California Universities for Earthquake Engineering). The second phase of the SAC project, also funded by FEMA, was a very substantial undertaking, and much more was learned. The profession and the steel industry will continue to feel profound effects of the Northridge event for years to come. For the reduced beam section (RBS) the beam flange width is reduced (by cutting) at a point away from the column face in order to force first yield at that point.

## Slide 35: Reduced Beam Section (RBS) Test Specimen SAC Joint Venture
Graphics courtesy of Professor Chia-Ming Uang, University of California San Diego
Notes: A beam-to-column joint test that utilizes the reduced beam section (RBS) detail is shown in the photograph. The experimental hysteresis plot is also shown. The RBS detail has been recognized as a pre-qualified connection in FEMA 350 and subsequent AISC documents. The behavior of this connection (actually member) detail is ductile and forces the inelasticity to occur in the beam section away from the beam-to-column welding and bolting. Graphics courtesy of Professor Chia-Ming Uang, University of California San Diego.

## Slide 36: T-stub Beam-Column Test SAC Joint Venture
Photo courtesy of Professor Roberto Leon, Georgia Institute of Technology
Notes: This slide shows a photo of a T-stub connection prior to testing. A hydraulic actuator was used to load the system, and the column was restrained by load sensing pins. A series of six beam-column tests that incorporated T-stubs very similar to those tested in a component test series were tested to failure. The beam-column tests were intended to provide benchmarks for relating the component test data to actual connections. Courtesy of Professor Roberto Leon, Georgia Institute of Technology and Professor James Swanson, University of Cincinnati.

## Slide 37: T-Stub Failure Mechanisms
Photos courtesy of Professor Roberto Leon, Georgia Institute of Technology
Plastic hinge formation -- flange and web local buckling
Net section fracture in stem of T-stub
Notes: Two of the beam-column tests failed when the stems of the T-stubs fractured as is shown in the left photo on this slide. Because the T-stubs failed before the beams, these two connections would be classified as partial strength. Four of the connections failed with plastic hinges forming in the beam as is shown in the photo on the right in this slide; these connections would be considered full strength. Also notice the severe flange and web local buckling of the beam. Courtesy of Professor Roberto Leon, Georgia Institute of Technology and Professor James Swanson, University of Cincinnati.

## Slide 38: T-Stub Connection Moment Rotation Plot
Graphic courtesy of Professor Roberto Leon, Georgia Institute of Technology
Rotation (rad)
-0.06
-0.04
-0.02
0.00
0.02
0.04
0.06
Moment (k-in.)
-7000
-6000
-5000
-4000
-3000
-2000
-1000
0
1000
2000
3000
4000
5000
6000
7000
Moment (kN-m)
-700
-600
-500
-400
-300
-200
-100
0
100
200
300
400
500
600
700
FS-03 – Moment-Rotation
Notes: This slide shows the moment-rotation curve obtained during the first beam-column test. The connection failed with a net section fracture of the bottom T-stub. The connection exhibited substantial rotation capacity and ductility. Notice, too, that there is relatively little pinching and that the loss of slip resistance is not as pronounced as it was in the component tests. Courtesy of Professor Roberto Leon, Georgia Institute of Technology and Professor James Swanson, University of Cincinnati.

## Slide 39: Extended Moment End-Plate Connection Results
Photo courtesy of Professor Thomas Murray, Virginia Tech
Notes: Photo is of a laboratory test specimen of an extended moment end-plate connection. Beam flanges have buckled. The “thick plate” behavior results in the development of a plastic hinge at the end of the stiffened section of the beam as the significant local flange and web buckling illustrate. The photograph is courtesy of Professor Thomas Murray, Virginia Tech.

## Slide 40: Extended Moment End-Plate Connection Results
Graphics courtesy of Professor Thomas Murray, Virginia Tech
Notes: Graphic shows moment-rotation plots. Left is moment vs total rotation; right is moment vs plastic rotation.
Hysteresis plots from an extended, stiffened, moment end-plate connection. Graphics courtesy of Professor Thomas Murray, Virginia Tech

## Slide 41: Ductility of Steel Frame Joints
Welded Joints
  Brittle fracture of weld
  Lamellar tearing of base metal
  Joint design, testing, and inspection
Bolted Joints
  Fracture at net cross-section
  Excessive slip
Joint Too Weak For Member
  Shear in joint panel
Limit States
Notes: Other failures not on slide were due to crushing or buckling of column web, distortion of column flange, or panel zone shear yielding or buckling.

## Slide 42: Multistory Frame Laboratory Test
Notes: Graphic shows elevation of frame with vertical loads indicated, as well as induced horizontal rotation. Hysteresis shows parallelogram behavior.
Load deflection plot for three-story, single-bay frame test. Heavier axial loads would limit stability at large lateral deflections.

## Slide 43: Flexural Ductility Effect of Axial Load
W12x36
Notes: Moment capacity depends on axial load. Diagram shows moment-curvature for three different eccentricities on short column. For small eccentricity very little rotation is developed. For the larger eccentricities much greater rotation occurs.

## Slide 44: Axial Strut Laboratory test
Notes: Plot of axial load versus axial deflection. The hysteretic shape is complicated and shows significant degradation on the compression side. On the tension side some degradation is also apparent, and larger displacements occur at each cycle.
Plot representative of column or brace. Plot of axial load versus axial deflection for low-to-medium slenderness member (L/r = 45). Tension in upper right quadrant and compression in lower left. Theoretical buckling load reached on only the first cycle. Note the degrading stiffness, decreasing compressive strength, and permanent set caused by tension yielding. Other testing has shown prevention of local buckling is crucial to maintaining any post-buckling strength.

## Slide 45: Cross Braced Frame Laboratory test
Notes: Graphic shows frame force-displacement behavior with significant pinching and larger displacements required at each cycle to achieve the full strength.
Overall performance of concentrically braced frame governed by axial behavior of braces. Frame has braces in both directions. Fatness of loops depends on slenderness of bracing members; lower slenderness ratios give fatter loops. Note the degrading stiffness.

## Slide 46: Tension Rod (Counter) Bracing Conceptual Behavior
H

“Slapback”
For cycle 2
H
Notes: Graphic shows cross-braced frame elevation and extremely pinched force-displacement diagram. Larger displacements required at each cycle to achieve the full strength, with zero resistance in the low-displacement range.
Tension ties stressed beyond yield experience permanent deformation. Each load reversal results in a further increment of deformation; structure moves, unrestrained, through larger range of motion. If braces do not have equal strength, structure will accumulate deflections in one direction, "racheting" sideways as cycles go on.

## Slide 47: Eccentrically Braced Frame
Notes: Graphic shows photograph of eccentrically braced frame (EBF) under construction. Photo from Modern Steel Construction.

## Slide 48: Eccentrically Braced Frame Lab test of link
Notes: Yield in eccentrically braced frames occurs in link (short portion of beam between braces). Shear yielding produces very fat and stable hysteresis loops. Braces, beams, and columns designed to remain elastic at load level that causes link yielding.

## Slide 49: Steel Behavior − Summary
Ductility
  Material inherently ductile
    Ductility of structure
        < ductility of member < ductility of material
  Achieved through detailing
Notes: Steels used in construction are typically extremely ductile materials. Ductility of the steel structure or system is less (sometimes many times less) than the ductility of the material because only a portion of material in the system will actually experience yielding. Damping is typically not high in steel structures, especially in welded structures. Bolted structures exhibit a higher degree of damping due to slip at connections. Unlike structures of other materials, the primary energy absorption mode in steel structures is yielding of members, usually in bending but sometimes in shear, axial tension, or compression.

## Slide 50: Steel Behavior − Summary
Damping
  Welded structures have low damping
  More damping in bolted structures due to slip at connections
  Primary energy absorption is yielding of members
Notes: Steels used in construction are typically extremely ductile materials. Ductility of the steel structure or system is less (sometimes many times less) than the ductility of the material because only a portion of material in the system will actually experience yielding. Damping is typically not high in steel structures, especially in welded structures. Bolted structures exhibit a higher degree of damping due to slip at connections. Unlike structures of other materials, the primary energy absorption mode in steel structures is yielding of members, usually in bending but sometimes in shear, axial tension, or compression.

## Slide 51: Steel Behavior − Summary
Buckling
  Most common steel failure under earthquake loads
  Usually not ductile
  Local buckling of portion of member
  Global buckling of member
Notes: Typical failure in steel structure subjected to earthquake is buckling, either global buckling of member, local buckling of portion of member, or global buckling of entire structure. Another potential weakness in steel structures is susceptibility to fracture; primarily a concern in heavy welded connections, members with notches, and in cold environments. The Northridge earthquake caused substantially more concern about fracture.

## Slide 52: Steel Behavior − Summary
Fracture
  Nonductile failure mode under earthquake loads
  Low-toughness heavy welded connections susceptible
  Net-section rupture
Notes: Typical failure in steel structure subjected to earthquake is buckling, either global buckling of member, local buckling of portion of member, or global buckling of entire structure. Another potential weakness in steel structures is susceptibility to fracture; primarily a concern in heavy welded connections, members with notches, and in cold environments. The Northridge earthquake caused substantially more concern about fracture.

## Slide 53: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Notes: Table of contents: Reference standards and design strength. The Provisions references commonly accepted codes for each material and indicates how requirements in those standards must be modified for use with the NEHRP Recommended Provisions seismic design procedure. Special additional provisions are also included in each materials chapter.

## Slide 54: Steel Design Specifications
AISC 341:
Seismic Design Provisions for Structural Steel Buildings
AISC 360:
Specification for Structural Steel Buildings
Notes: Graphic shows covers of the AISC Steel Construction Manual and Seismic Design Manual.
The referenced standard for structural steel (hot rolled shapes and plates, and sections built up from hot rolled shapes and plates) is the Specification for Structural Steel Buildings, (2016). The specification governing seismic design of steel buildings is Seismic Provisions for Structural Steel Buildings.
The pictured copies are the Manuals using the 2010 Specification and Seismic Provisions, as the Manuals based on the 2016 editions will not be available in print until 2017 and 2018.

## Slide 55: Using Reference Standards Structural Steel
Both the AISC LRFD and ASD methodologies are presented in a unified format in both the Specification for Structural Steel Buildings and the Seismic Provisions for Structural Steel Buildings.
Notes: Slide discusses reference standards.

## Slide 56: Cold Formed Steel Standard
Notes: Graphic shows cover of AISI North American Specification for the Design of Cold-formed Steel Structural Members .
Reference standard for cold formed steel is the AISI North American Specification for the Design of Cold-formed Steel Structural Members (shown on slide). It includes both ASD and LRFD.

## Slide 57: Other Steel Members
Steel Joist Institute
Standard Specifications, 2010
Steel Cables
ASCE 19-2010
Steel Deck Institute
Diaphragm Design Manual, DDM04, 2015
Notes: For design of other specialized steel members, the Provisions refers user to standards published by Steel Joist Institute and the ASCE 19 standard for cables. The Provisions indicates how SJI allowables should be increased to maximum strengths for use in seismic resistant design and give guidelines for modification of cable allowables. Note the Steel Deck Institute’s Diaphragm Design Manual is no longer referenced in the Provisions although it is a good source (do not use the 2.75 “factor of safety”). There are also other sources for steel deck diaphragms.

## Slide 58: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Notes: Table of contents: Moment resisting frames.

## Slide 59: Steel Moment Frame Requirements
Notes: i is shorthand for the total (elastic plus inelastic) rotation at the beam-to-column connection. Elastic drift at yield is on the order of 0.01 radians. The capacity is very sensitive to detail; thus, the requirement for testing representative joints. AISC Seismic includes an appendix with a testing protocol.

## Slide 60: Moment frames
Fuses
Encourage
Avoid
Encourage
  Flexural hinging in beams
Avoid
  Flexural hinging in columns
    (occurs at base)
  Connection failure
  Excessive column panel-zone yielding
Notes: Graphic shows:
Diagram of moment frame with plastic hinges in beams at every level.
Diagram of moment frame with plastic hinges in columns at the top and bottom of the first level.

## Slide 61: Steel Moment Frame Connections
sh
½ Lh
Mf
Mpr
Notes: Graphic shows:
Diagram of moment-frame beam-to-column connection.
Beam moment diagram with moment at column face and moment at expected plastic-hinge location noted.
This illustrates one aspect of the problem with the welded joint. The old connection usually must develop its flexural strength solely through the flange welds at the face. The moment is somewhat higher than Mp in order to develop an appreciable hinge in the beam. The larger moment and the reduced section both increase the demand stress above the actual yield of the beam. The number 1.7 is derived from common proportions for the contribution of the flange to the total plastic section modulus and the ratio of hinge length to inflection point distance plus overstrength commonly found in A36 steel (which is no longer the steel of choice for hot-rolled W shapes.) Additional issues include the geometric stress concentration, weld imperfections, shear lag from beam web to flange tip, residual stresses from welding heat, loss of ductility where triaxial tension exists, etc.

## Slide 62: Panel Zones
Special and intermediate moment frame:
Shear strength demand:
  1.1 to 1.4RyMp of beams
  Thickness (for buckling)
  Use of doubler plates
  (not economical, try to increase col. size instead)
Notes: Graphic shows:
Beam-column connection with beam moments acting on column shown.
Panel shear often controls, and this may require larger column or "doubler" plate on web, which is expensive to fabricate. SAC testing has shown that panel zone yield contributes to fracture of beam flange welds, apparently due to the concentration of strains at that location. However, some yielding in the panel zone is considered to be a good way to dissipate energy. The final SAC recommendations require that the yield strength of the shear panel zone be at least strong enough to reach the beginning of yield in the beam flexural hinge areas but not full development of the flexural hinge.

## Slide 63: Panel zone strength
*
*
AISC 360 J10.6 | Low axial force | High axial force
Panel zone deformation not modeled |  | 
Panel zone deformation modeled |  | 

## Slide 64: Panel zone strength
Axial force
  High axial force rare for moment-frame columns
Panel zone deformations
  Seismic panel zone shear demand is often independent of panel zone modeling
    Based on (beam) member strength
    Unlike wind, stability
  Panel zone (seismic) deformations required to be included (per codes)

## Slide 65: Steel Moment Frames
Beam shear: 1.15RyMp + gravity
Beam local buckling
  Smaller b/t than for plastic design
Continuity plates for smaller columns
Strong column - weak beam rule
  Prevent column yield except in panel zone
  Exceptions: Low axial load, strong stories, top story, and non-SFRS columns
Notes: Note the tighter restrictions on b/t and h/t than required for plastic design. Beam flange continuity plates are now required if included in the test specimens. It is not an analytical check. The b/t limit rules out a few common beam shapes for grade 50 steel.

## Slide 66: Steel Moment Frames
Lateral support of column flange requirements
  Top of beam if column elastic
  Top and bottom of beam otherwise
  Amplified forces for unrestrained
Lateral support of beams requirements
  Both flanges
  Spacing < 0.095ryE/RyFy
Notes: Limits to prevent member buckling. The limit is for special frames and it is different from the general limits in the main spec, which applies to the compression flange and depends on the square root of Fy. The Commentary to the AISC 341 includes the following:
“Spacing of lateral braces for beams in SMF systems is specified not to exceed 0.086 ry E / Fy. This limitation, which is unchanged from previous editions, was originally based on an examination of lateral bracing requirements from early work on plastic design and based on limited experimental data on beams subject to cyclic loading. Lateral bracing requirements for SMF beams have since been investigated in greater detail in Nakashima, Kanao and Liu (2002). This study indicates that a beam lateral support spacing of 0.086ryE/Fy is appropriate, and slightly conservative, to achieve an interstory drift angle of 0.04 radian.”

## Slide 67: Prequalified Connections
ANSI/AISC 358, Prequalified Connections for Special and Intermediate Steel Moment Frames for Seismic Applications
  Reduced Beam Section Connections
  Bolted Stiffened and Unstiffened Extended Moment End Plate Connections
  Bolted Flange Plate
  Welded Unreinforced Flange-Welded Web (WUF-W)
  Kaiser Bolted Bracket
  CONXL
Notes: FEMA 350 resulted from the SAC Joint Venture project. Subsequently, an ANSI/AISC committee was established to create ANSI/AISC 358. The work by this committee is continuing and additional connections are being addressed. The ANSI/AISC 358 standard is available for download from the AISC website.

## Slide 68: Reduced Beam Section (RBS)
Notes: Graphic shows:
Plan section and elevation section of RBS connection, with flange reductions in the beam indicated.
The slide illustrates a beam-to-column connection using the reduced beam section (RBS) connection. The beam flanges and shear plate are welded to the column. The reduction of the beam section forces hinging to occur in the beam away from these connection details.

## Slide 69: Reduced beam section
Beam intentionally weakened to create controlled yielding
Connection at face of column stronger than reduced section
Capacity design ensures good performance
Reduction in stiffness
Potential reduction in stability
Notes: Graphic shows:
Plan section and elevation section of RBS connection, with flange reductions in the beam indicated.

## Slide 70: Bolted End Plate
Notes: Graphic shows three variants of the extended moment end-plate connection:
4-bolt unstiffened;
4-bolt stiffened;
8-bolt stiffened;
The slide illustrates an extended moment end-plate connection.

## Slide 71: Bolted end plate
End-plate connection at column face
  Stronger than beam
  Capacity design
    Flexural yielding of plate
    Bolt tension
    Weld tension
    Weld shear
    etc.
Notes: Graphic shows three variants of the extended moment end-plate connection:
4-bolt unstiffened;
4-bolt stiffened;
8-bolt stiffened;

## Slide 72: Welded unreinforced flange, welded web (WUF-W)
Notes: Graphic shows welded unreinforced flange, welded web connection.

## Slide 73: WUF-W
Welded web
Improved materials
  Toughness
  Limited tensile strength
Improved welding details
  Restraint relief provided by special access hole
  Backing details
  Removal of weld tabs
Improved QA/QC
Notes: Graphic shows welded unreinforced flange, welded web connection.

## Slide 74: Bolted Flange Plates
Notes: Graphic shows bolted flange-plate connection.
Slide illustrates a beam-to-column connection using welded cover plates on the beam flanges.

## Slide 75: Bolted flange plate
Beam is fuse
Flange plates transfer moment to column
Web does not participate in transferring moment
Multiple bolt-related limit states
Notes: Graphic shows bolted flange-plate connection.

## Slide 76: Bolted flange plate
Beam is fuse
Flange plates transfer moment to column
Web does not participate in transferring moment
Multiple bolt-related limit states
Notes: Graphic shows bolted flange-plate connection.

## Slide 77: Kaiser Bolted Bracket
Notes: Graphic shows Kaiser Bolted bracket connection.

## Slide 78: Kaiser Bolted bracket
Proprietary
High-strength cast-steel brackets
Configuration
  Bolted or welded to beam
  Bolted to column
Similar to Bolted Flange Plate
  Beam expected to yield
Capacity design used for
  Bracket
  Column
  Local limit states in beam
Notes: Graphic shows Kaiser bolted brackets of different sizes.

## Slide 79: CONXL (ConXtech)
Notes: Graphic shows three-dimensional diagram of square HSS column with 4 beams connecting. CONXL end hardware is visible.

## Slide 80: CONXL (ConXtech)
Proprietary
2-way system
Bolted collars
16” concrete-filled box columns
RBS if required
  (to meet strong-column/weak-beam)
Beam expected to yield
  Capacity design
  Consideration of both axes
Notes: Graphic shows three-dimensional diagram of square HSS column with 4 beams connecting.
Graphic shows HSS column with connecting hardware.

## Slide 81: Welded Flange Plates (not prequalified)
Notes: Graphic shows welded flange-plate connection.
Slide illustrates a beam-to-column connection using welded cover plates on the beam flanges.

## Slide 82: Free Flange Connection (not prequalified)
Notes: Graphic shows the free-flange connection.
Slide illustrates a beam-to-column connection using welded cover plates on the beam flanges. Prequalified connections may be used with qualification testing, which may be project-specific, or may utilize tests reports that are available publically (such as some university research reports).

## Slide 83: Excellent Moment Frame Behavior
Notes: Graphic shows force-displacement diagram for a moment connection test Hysteresis loops are full, with slight degradation at larger displacements.
This slide illustrates excellent moment frame behavior as noted by the large, full hysteresis loops that exhibit very little strength degradation out to a plastic rotation of approximately 0.04 rad. The test was of a cover plated beam with fully welded web conducted at the University of Texas under the direction of Professor Michael Engelhardt

## Slide 84: Excellent Moment Frame Behavior
Notes: The photograph is of a welded bottom haunch connection that exhibits excellent hysteretic behavior. The test was conducted at the University of California at San Diego under the direction of Professor Chia-Ming Uang.
Graphic shows: Photograph of haunched beam test specimen. Yielding and buckling of the flanges outside the haunch region is visible.
Hysteresis diagrams for the test specimens. Hysteresis loops are full, with slight degradation at larger displacements.

## Slide 85: Excellent Moment Frame Behavior
Notes: The photograph is of a welded top and bottom haunch connection that exhibits excellent hysteretic behavior. The test was conducted at the University of California at Berkeley under the direction of Andrew Whitaker and Vitelmo Bertero.
Graphic shows: Photograph of haunched beam test specimen. Yielding and buckling of the flanges outside the haunch region is visible.
Hysteresis diagrams for the test specimens. Hysteresis loops are full, with slight degradation at larger displacements.

## Slide 86: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Seismic design category requirement
Moment resisting frames
Braced frames
Notes: Table of Contents: braced frames.

## Slide 87: Concentrically Braced Frames Basic Configurations
K
V
(Chevron)
Inverted V
(Chevron)
K
Diagonal
X
Notes: Graphic shows:
Six frames with different brace configurations.
K bracing will introduce bending into columns following buckling of compression brace and is often prohibited. V and inverted V bracing require continuity of beams.

## Slide 88: Braced Frame Under Construction
Notes: A braced frame using inverted V type bracing is shown under construction.

## Slide 89: Braced Frame Under Construction
Notes: Braced frame using diagonal bracing under construction.
Note that this braced frame has multiple tiers that are not at floor or roof levels. This is thus a multi-tiered braced frame that requires special attention to column stability.

## Slide 90: Concentrically Braced Frames
Special AISC Seismic R = 6
AISC 341 Section F2
Ordinary AISC Seismic R = 3.25
AISC 341 Section F1
Not Detailed for Seismic R = 3
AISC 360
Notes: The special and ordinary systems are similar. Chapter F.1 and Chapter F.2 refer to sections AISC 341.

## Slide 91: Concentrically braced frames
Fuses
Encourage
  Yielding of braces
  Buckling of braces
Avoid
  Flexural hinging in columns (story mechanisms)
  Buckling of beams or columns
  Connection failure
Notes: Graphic shows concentrically braced frames:
With braces at all levels buckling or yielding;
With braces buckling or yielding at the first level only and columns with plastic hinges at that level;
With column buckling at the first level; and
With brace connections fracturing at the first level and columns with plastic hinges at that level;

## Slide 92: Brace cyclic behavior
Pcr
Ry Ag Fy
Compression
Tension
Notes: Plot of axial load versus axial deflection. The hysteretic shape is complicated and shows significant degradation on the compression side. On the tension side some degradation is also apparent, and larger displacements occur at each cycle.

## Slide 93: Concentrically Braced Frames
Dissipate energy after onset of global buckling by avoiding brittle failures:
  Minimize local buckling
  Strong and tough end connections
  Better coupling of built-up members
Notes: Most common failures were from: (1) fracture at local buckling where global buckling created a hinge and (2) fracture at connections.

## Slide 94: Concentrically Braced Frames Special and Ordinary
Bracing members:
- Compression capacity = Pn
- Slenderness:
  Ordinary (chevron configuration):
  Special: KL/r ≤ 200

## Slide 95: Concentrically Braced Frames Special and Ordinary
Bracing members:
Width / thickness limits
  Generally compact
  Angles, tubes and pipes very compact
Special:
  Balanced tension and compression
Notes: “Balanced” tension and compression means that the sum of horizontal components of tension braces is between 30% and 70% of total horizontal force. This check is a design level, not post-buckling level. It is intended to prevent the “racheting” accumulation of inelastic deformation in one direction and the “impact” possible in a “slapback” phenomenon.

## Slide 96: Concentrically Braced Frames Special concentrically braced frames
Brace connections
Axial tensile strength > smallest of:
  Axial tension strength = RyFyAg
  Maximum load effect that can be transmitted to brace by system
Axial compressive strength  1.1Pne, where Pne is the compressive strength based on RyFy.
Flexural strength > 1.1RyMp or rotate to permit
brace buckling while resisting AgFcr
Notes: These requirements are all for special concentrically braced frames. Block shear and tensile rupture on net section must both be considered. Refer to the AISC 341 for ordinary concentrically braced frame details.

## Slide 97: Concentrically Braced Frames
V bracing:
  Design beam for D + L + unbalanced brace forces, using 0.3 Pne for compression and RyFyAg in tension
  Laterally brace the beam
  Beams continuous between columns
K bracing:
  Not permitted
Notes: Graphic shows diagrams of braced frames:
Chevron (inverted V) configuration;
K configuration
Limits on use and design of V and K braces. Refer to Sec. F2.4 in the AISC 341 for additional description. The following text is taken from the Commentary to the AISC 341. Refer to the Commentary for additional information and description of the behavior.
“V-braced and inverted-V-braced frames exhibit a special problem that sets them apart from braced frames in which both ends of the braces frame into beam-column connections. The expected behavior of SCBF is that upon continued lateral displacement as the brace in compression buckles, its force drops while that in the brace in tension continues to increase up to the point of yielding. In order for this to occur, an unbalanced vertical force must be resisted by the intersecting beam as well as its connections and supporting members. In order to prevent undesirable deterioration of lateral strength of the frame, the SCBF provisions require that the beam possess adequate strength to resist this potentially significant post-buckling load redistribution (the unbalanced load) in combination with appropriate gravity loads.”
Graphic shows diagrams of braced frames:
Chevron (inverted V) configuration;
K configuration

## Slide 98: Concentrically Braced Frames
Built-up member stitches:
  Spacing < 40% KL/r
  No bolts in middle quarter of span
  Minimum strengths related to Py
Column in CBF:
  Same local buckling rules as brace members
  Splices resist moments
Notes: The following text is taken from the Commentary to the AISC 341. Closer spacing of stitches and higher stitch strength requirements are specified for built-up bracing members in SCBF than those required for OCBF. These are intended to restrict individual element bending between the stitch points and consequent premature fracture of bracing members. Wider spacing is permitted under an exception when buckling does not cause shear in the stitches. Bolted stitches are not permitted within the middle one-fourth of the clear brace length as the presence of bolt holes in that region may cause premature fractures due to the formation of a plastic hinge in the post-buckling range.

## Slide 99: Plastic mechanism analyses
Case 2
Case 1
Frame
Design forces
Compression
Brace
Tension
Brace
Displacement
Force
Displacement
Force
Notes: Graphic shows:
Frame elevation with force-displacement diagrams for tension and compression braces.
Frame.
Frame under design forces. Brace axial forces are less than their full strength.
Case 1. Braces in tension at full yield and braces in compression at their full buckling strength.
Case 2. Braces in tension at full yield and braces in compression having reduced force.

## Slide 100: Plastic mechanism analyses
Ry Fy Ag
1.14 Fcre Ag
Ry Fy Ag
1.14 Fcre Ag
Ry Fy Ag
1.14 Fcre Ag
Ry Fy Ag
1.14 Fcre Ag
Case 1
Notes: Graphic shows:
Diagram of case 1, with braces in tension at full yield and braces in compression at their full buckling strength. Brace actions are shown as forces acting on the frame.

## Slide 101: Plastic mechanism analyses
0.342 Fcre Ag
Ry Fy Ag
0.342 Fcre Ag
Ry Fy Ag
0.342 Fcre Ag
Ry Fy Ag
0.342 Fcre Ag
Ry Fy Ag
Case 2
Notes: Graphic shows:
Diagram of Case 2. Braces in tension at full yield and braces in compression having reduced force. Brace actions are shown as forces acting on the frame.

## Slide 102: Eccentrically Braced Frames
Link
Brace
Beam
Notes: Graphic shows eccentrically braced frames, with braces, beams and links identified.
Eccentrically braced frames. Define terms.

## Slide 103: Eccentrically braced frames
Fuses
Encourage
  Yielding of link
Avoid
  Flexural hinging in columns (story mechanisms)
  Buckling of braces, beams or columns
  Connection failure
Notes: Graphic shows eccentrically braced frames:
With links at all levels yielding;
With link yielding at the first level only and columns with plastic hinges at that level;
With column buckling at the first level; and
With brace connections fracturing at the first level and columns with plastic hinges at that level;

## Slide 104: Buckling-Restrained Braced Frames (BRBFs)
Type of concentrically braced frame
Beams, columns and braces arranged to form a vertical truss. Resist lateral earthquake forces by truss action
Special type of brace members used: Buckling-Restrained Braces (BRBs). BRBS yield both in tension and compression - no buckling !!
Develop ductility through inelastic action (cyclic tension and compression yielding) in BRBs.
System combines high stiffness with high ductility
Notes: BRBFs are concentrically braced frames, consisting of beams, columns and braces arranged to form a truss. BRBFs resist lateral load primarily through truss action, with member response dominated by axial force (tension and compression).
Unlike conventional concentrically braced frames, BRBFs are constructed with a special type of brace member: Buckling-Restrained Braces (BRBs).
BRBs have the unique quality that they do not buckle when loaded in compression. Consequently, BRBs yield in a ductile manner in both tension and compression. The use of BRBs results in a frame that combines high elastic stiffness with excellent ductility.
BRBFs are considered to be a high ductility framing system, and is assigned high R-factors in ASCE-7.
Per ASCE-7, the R-factors for BRBFs are: R=7 for BRBF with non-moment resisting beam-to-column connections.
R=8 for BRBF with moment resisting beam-to-column connections.
These are the same as the R-factors assigned to EBFs.

## Slide 105: Buckling-Restrained Braced Frames (BRBFs)
Steel Core
Casing
Buckling- Restrained Brace: Steel Core + Casing
Notes: Graphic shows:
Buckling-restrained brace assembly diagram;
Casing; and
Steel core.
The key feature of a BRBF is the use of Buckling-Restrained Braces (BRBs).
A BRB consists of a steel core and a casing. The casing covers the steel core.

## Slide 106: Buckling-Restrained Braced Frames (BRBFs)
Debonding material
Steel Core
Steel jacket
Mortar
Casing
Buckling- Restrained Brace: Steel Core + Casing
A
A
Notes: Graphic shows a BRB assembly and a cross section, The cross section has a steel core, debonding material, mortar, and a steel jacket.
The are a number of different configurations for BRBs. This slide shows one possibility. The steel core is simply a rectangular plate. The casing, which restrains buckling of the core, is typically constructed of a mortar filled steel tube. The steel core is surrounded by a debonding material that decouples the steel core from the casing, for purposes of resisting axial force. That is, the debonding material is intended to prevent transfer of axial stress from the steel core to the casing. Consequently, the casing essentially "floats" on the steel core.
There are a number of possible configurations for the shape of the steel core. In addition to a single plate, BRBs have been constructed using cruciform shaped plates, or a pair of plates or shapes.

## Slide 107: Buckling-Restrained Braced Frames (BRBFs)
P
P
Steel core resists entire axial force P
Casing is debonded from steel core
  - casing does not resist axial force P - flexural stiffness of casing restrains buckling of core
Notes: Graphic shows:
Buckling-restrained brace assembly diagram;
The concept of the BRB is that the steel core resists the applied axial force P. The debonding material that surrounds the core is intended to prevent the casing from carrying axial force. Since the casing has no (or very little) axial force, its full flexural stiffness is available to resist buckling of the steel core.

## Slide 108: Buckling-Restrained Braced Frames (BRBFs)
Core projection and brace connection segment
Steel Core
Yielding Segment
Buckling- Restrained Brace: Steel Core + Casing
Notes: Graphic shows:
Buckling-restrained brace assembly diagram;
Steel core.
The central section of the steel core, as shown in the slide, is intended to be the portion of the core that yields in tension and in compression. At the ends of the BRB, the core projects outside of the casing. This core projection typically has a significantly larger cross-sectional area than the yielding segment, and is usually reinforced to prevent buckling of the projection. Further, the core projection is normally prepared with bolt holes or other features that allow connection of the BRB to the remainder of the frame.
A building designer using a BRBF does not normally develop the detailed design of a buckling restrained brace, such the shape of the core and core projections, the details of the casing and debonding material, and the connection details provided on the core projection.
Rather, there are companies that manufacture and sell BRBs. These are proprietary and patented designs which have undergone design development and testing by the manufacturers. Thus, the building designer will normally specify the required strength and stiffness of the BRBs, and the manufacturer will supply BRBs that meet these specifications.
At present (2016) there are two manufacturers that market BRBs in the US:
- CoreBrace (http://www.corebrace.com/)
Nippon Steel Corporation (http://www.unbondedbrace.com/)

## Slide 109: Brace Behavior Under Cyclic Axial Loading
P


P
Py
PCR
Conventional Brace:
yields in tension (ductile)
buckles in compression (nonductile)
significantly different strength in tension and compression
Notes: Graphic shows:
Force-displacement diagram for a buckling brace.
Diagram of a brace in compression undergoing flexural buckling.
This slide reviews the behavior of a conventional brace when subjected to cyclic axial load.
A conventional brace buckles when loaded in compression, resulting in deterioration of strength and stiffness. A conventional brace exhibits significantly different strengths in compression and tension.

## Slide 110: Brace Behavior Under Cyclic Axial Loading
P

Py
PCR
Py

Buckling-Restrained Brace:
yields in tension (ductile)
yields in compression (ductile)
similar strength in tension and compression (slightly stronger in compression)
Notes: Graphic shows:
Force-displacement diagram for a buckling-restrained brace.
Diagram of a buckling-restrained brace in compression undergoing axial yielding.
A buckling-restrained brace yields in a ductile manner, both in tension and in compression. As a result, a BRB exhibits highly desirable behavior as an energy-dissipating element in a seismic-resistant frame.
A BRB also exhibits very similar strengths in compression and in tension. This avoids many of the difficulties that result from large unbalanced brace forces in SCBFs, such as the difficulty in designing beams in inverted-V braced SCBFs.
Tests show that BRBs exhibit slightly higher strength in compression than in tension. The maximum compression strength of a BRB may be on the order of 3 to 10-percent greater than the maximum tension strength of the BRB. This higher measured compression strength may be due to partial engagement of the casing in resisting axial force, when the BRB is loading in compression. This partial engagement of the casing may be due to imperfect debonding, resulting from expansion of the core in compression (Poisson's effect) and higher mode buckles (ripples) in the core that cause the core to press against the casing.

## Slide 111: Bracing Configurations for BRBFs
Two Story X- Bracing
V- Bracing
X- Bracing
Inverted V- Bracing
Single Diagonal
Notes: Graphic shows five frame elevations:
Single diagonal; Inverted V- Bracing; V- Bracing; X- Bracing, and 2-story X- Bracing. X bracing is barred.
Various bracing arrangements are possible for BRBFs, as is the case with conventional braced frames.
Single story X-bracing is generally not possible for BRBFs because of the difficulty in crossing the two BRBs at their centers. Also, K-braced BRBFs are not permitted (see Section F4.4).

## Slide 112: Preliminary Design of Braces
Design braces precisely to calculated capacity
(Pu = fPn = fFyAsc)
F
q
y
u
sc
F
P
A
f
=
q
cos
2
F
P
u
=
Assume braces resist 100% of story shear
Notes: Graphic shows V-braced frame with lateral load undergoing racking. The angle alpha is measured between the brace and the horizontal.
Preliminary design of braces.

## Slide 113: Preliminary Design of Braces
d
dbr
Ly
Lwp
e~(dbr/Lwp)(Lwp/Ly)
Lwp
K~EAsc/Ly
= CkEAsc/Lwp
1.2 ≤ Ck ≤ 1.8
Notes: Graphic shows: V braced frame, and diagram of the non-prismatic steel core. Work-point-to-workpoint length (Lwp) and length of yielding zone (Ly) are indicated.
Preliminary design of braces.

## Slide 114: Buckling restrained braced frames
Fuses
Encourage
  Yielding of braces
Avoid
  Flexural hinging in columns (story mechanisms)
  Buckling of beams or columns
  Connection failure
Notes: Graphic shows buckling-restrained braced frames:
With braces at all levels yielding;
With braces yielding at the first level only and columns with plastic hinges at that level;
With column buckling at the first level; and
With brace connections fracturing at the first level and columns with plastic hinges at that level;

## Slide 115: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Braced frames
Other topics
Notes: Table of contents: other topics.

## Slide 116: Special Truss Moment Frame
Buckling and yielding in special section
Design to be elastic outside special section
Deforms similar to EBF
Special panels to be symmetric X or Vierendeel
Notes: Graphic shows elevation of Special truss moment frame. Bay length (L), length of special segment (Ls), and length of panel (Lp) are indicated.
Special truss moment frames are a new introduction to seismic resistant construction. The concept is that a set of panels near midspan of horizontal trusses, where the gravity load shear is low, are design to yield and buckle in a controlled manner to dissipate energy of strong ground shaking. It should be anticipated that the bucked members may have to be replaced following strong ground shaking.

## Slide 117: Special Truss Moment Frame
Geometric Limits:
Notes: Graphic shows elevation of Special truss moment frame. Bay length (L), length of special segment (Ls), and length of panel (Lp) are indicated.
The system has been tested, but only a few real buildings have yet been constructed. The geometric limits are mostly based upon the tested specimens. The use of flat bar diagonals in the special panels prevents local buckling problems.

## Slide 118: Special Truss Moment Frame
Notes: Graphic shows free body diagram of special segment, with shear (Vp) and moments at each end.
The special section is shown. The plastic shear capacity depends on flexural hinging of the chords at the ends of the section and the buckling and tensile yield capacities of the webs. The plastic shear demand is directly related to the horizontal forces on the structure. The angle between the diagonal and the chord is given as .

## Slide 119: Special Truss Moment Frame
Notes: Two photos of special truss moment frame experimental test specimen. Special segments have cross-braced panels.
This specimen was part of a research program at the University of Michigan under the direction of Professor Subash Goel. This research led to the inclusion of the STMF as a recognized structural system in the NEHRP Recommended Provisions. Photo courtesy of Nucor Research and Development.

## Slide 120: Special Truss Moment Frame
Notes: Photograph of Special truss moment frame under construction. Special segments have Vierendeel panels.

## Slide 121: General Seismic Detailing
Materials:
  Limit to lower strengths and higher ductilities
Bolted Joints:
  Fully tensioned high strength bolts
  Class-A (or better) faying surface)
  Limit on bearing
Notes: Seismic detailing per AISC Seismic is more than simply the rules for the specific systems. There are also general rules for several subjects that apply to all types of steel seismic resisting systems.

## Slide 122: General Seismic Detailing
Welded Joints:
  AWS requirements for welding procedure specs
  Filler metal toughness
    CVN > 20 ft-lb @ 0°F
  Warning on discontinuities, tack welds, run offs, gouges, etc.
Columns:
  Strength using o
  Splices: Requirements on partial penetration welds and fillet welds
Notes: The requirements for weld metal toughness are new. The reference to AWS welding procedure specs is a new emphasis. It is likely that structural engineers will have to become more well educated about welding in the future. The rules on columns are intended to prevent premature failure in these vulnerable components.

## Slide 123: Welded Shear Studs
Notes: Photo (1) shows flexural testing of beam with composite deck. Photo (2) shows worker installing shear studs with gun-type stud-welding device on a steel deck in a building under construction.
Welded shear studs have been a part of the AISC Specifications since 1961. Beginning in the late 1980s, the strength model for shear studs used in cold-formed steel deck begin to come under scrutiny. In particular, the reduction factor, which was a function of deck geometry, in the AISC specifications was thought to be unconservative and in need of change. Research teams from several places around the world were working on the problem. This was in part due to the fact that the AISC procedures had been widely adopted. A series of beam tests and several hundred push-out tests were conducted at Virginia Tech over a number of years. This comprehensive research program led to changes in the AISC specification. These changes will be highlighted in the following slides.

## Slide 124: Shear Stud Strength - AISC Specification
Qn = 0.5 Asc ( fc’ Ec)1/2  Rg Rp Asc Fu
Rg = stud geometry adjustment factor
Rp = stud position adjustment factor
f = 0.65 (per AISC 360, Section I8.3)
Notes: The shear stud strength model is no longer a direct function of the deck geometry, although the limitations of the empirical based formulation is a function of the deck depths that were used in the study. The reader is referred to the AISC specification and commentary for a more complete discussion. The flexural design procedure is unchanged, other than the calculation of the shear stud strength. The strength reduction factor for bending has been increased from 0.85 to 0.9. This reflects the use of a more accurate shear stud strength model. As in past specifications, there is no strength reduction factor applied separately to the shear studs.

## Slide 125: Qn = 0.5 Asc ( fc’ Ec)1/2  Rg Rp Asc Fu Rg = stud group adjustment factor
*0.85 if wr /hr < 1.5
Rg = 0.7
Rg = 0.85
Rg = 1.0*
Rg = 1.0
  Shear Studs
  Group Adjustment Factor
Notes: Graphics show:
Beam with single stud through deck (flutes transverse to beam axis).
Beam with single stud through deck (flutes parallel to beam axis).
Beam with two studs through deck (flutes transverse to beam axis).
Beam with three studs through deck (flutes transverse to beam axis).
This slide illustrates the application of the group adjustment factor, Rg. The first, third, and fourth figures illustrate “beam” applications – that is the deck is perpendicular to the steel section. The second figure illustrates a “girder” for which the deck is parallel to the steel section. A narrow rib in the girder application, as defined by the wr /hr ratio being less than 1.5, results in a reduction in Rg to a value of 0.85.

## Slide 126: Qn = 0.5 Asc ( fc’ Ec)1/2  Rg Rp Asc Fu Rp = stud position adjustment factor
Rp = 0.75
Deck parallel
Rp = 1.0
No Deck
Rp = 0.75 (strong)
= 0.6 (weak)
Deck perpendicular
  Shear Studs
  Position Adjustment Factor
Notes: Graphics show:
Beam with single stud through deck (flutes transverse to beam axis).
Beam with single stud through slab (no steel deck)
Beam with single stud through deck (flutes parallel to beam axis).
This slide illustrates the applications of the position adjustment factor. Refer to AISC for a further description of the “no deck” and “deck” cases for the “girder” applications in the second and third figure. The recommended value of Rp for the beam case, illustrated in the first figure, is the weak position case of 0.6. Use of the higher value of 0.75 requires close control and inspection during the stud installation process during construction. This control is difficult to obtain.

## Slide 127: Quality and Welding
AISC 341
  Appendix Q
    Basic Quality Assurance Plan
    Inspection tables
      Welding
      Bolting
  Appendix W
    Welding quality
      Details
      Inspection

## Slide 128: Quality and Welding
AISC 341
  Addresses:
    Quality Control - Fabricator/Erector
    Quality Assurance - Owner
    Non-Destructive Testing
  Uses:
    Observe and Perform (AISC Seismic Provisions)

## Slide 129: Q5.1. Visual Welding Inspection
Notes: Graphics show:
AISC Table (Visual inspection tasks before welding)

## Slide 130: Q5.1. Visual Welding Inspection
Notes: Graphics show:
AISC Table (Visual inspection tasks during welding)

## Slide 131: Q5.1. Visual Welding Inspection
Notes: Graphics show:
AISC Table (Visual inspection tasks after welding)

## Slide 132: Q5.3. Inspection of Bolting
Notes: Graphics show:
AISC Table (Visual inspection tasks prior to bolting)
AISC Table (Visual inspection tasks during to bolting)

## Slide 133: Q5.3. Inspection of Bolting
Notes: Graphics show:
AISC Table (Visual inspection tasks after bolting)

## Slide 134: Q5.4. Other Inspections
See table for other inspection tasks related to
  Reduced beam section requirements
  Protected zone
Notes: Graphics show:
AISC Table (other inspection tasks)

## Slide 135: AISC 341 QA
NDT
  CJP > 5/8”,
    UT 100%
      May be adjusted downward based on job performance.
    MT 25% of beam flange to column flange welds
  Thick T CJP joints
    tcf > 1.5”
    tbf > 0.75”
    UT after welding

## Slide 136: Inspection and Testing Base Metal Testing
More than 1-1/2 inches thick
Subjected to through-thickness weld shrinkage
Lamellar tearing
Ultrasonic testing
Notes: Base metal testing required: where base metal more than 1-1/2 in. thick subjected to through-thickness weld shrinkage (lamellar tearing is possible); ultrasonic testing required to identify presence of discontinuities in base metal.

## Slide 137: AISC 341 QA
NDT
  MT weld tab removal sites
    Except at continuity plates
  Weld access holes
    SMF connections
    Splices

## Slide 138: Inspection and Testing Shop Certification
Domestic:
  AISC
  Local jurisdictions
Foreign:
  No established international criteria
Notes: AISC can certify fabricating shops. Program includes scheduled and surprise inspections to review quality control procedures, personnel, and results. Some local jurisdictions have adopted similar certification procedures. As there is no internationally accepted quality certification, foreign fabricated steel should be given close inspection.

## Slide 139: NEHRP Recommended Provisions Steel Design
Context in Provisions
Steel behavior
Reference standards and design strength
Moment resisting frames
Braced frames
Other topics
Notes: Summary

## Slide 140: Questions
Notes: Slide to initiate questions from the participants.

## Slide 141: Chapter 9: Structural Steel Design
Part 2: Design Examples

## Slide 142: Chapter 9: Structural Steel Design
Part 2: Design Examples:
Special Moment Frame

## Slide 143: Special Moment Frames Seven Story Office Building, Los Angeles
Perimeter Moment Frames, all bays engaged
SDS=1.0
SD1=0.6
Occupancy Category II
Seismic Design Category D
Design Parameters (Table 12.2-1)
  R=8
  Cd=5.5
  W0=3.0
Notes: The information on the following several slides are taken from Example 6.2 (Alternate A) of the NEHRP Design Examples volume (FEMA 1051). FEMA 1051 was written based on the 2015 NEHRP Recommended Provisions. The example complies with the AISC 341.

## Slide 144: Special Moment Frame Example
Structural Materials:
  Concrete (all floors) = 3.0 ksi lightweight
  Other Concrete = 4.0 ksi normal weight
Steel:
  Wide Flange Sections= ASTM A992 Grade 50
  HSS= ASTM A500 Grade B
  Plates= ASTM A36
Notes: Structural Materials

## Slide 145: Special Moment Frames Plan of Building
Notes: Graphic shows: a full floor plan of the building. There are seven bays in the E-W direction and five bays in the N-S direction. The design is illustrated for loads acting in the E-W direction.

## Slide 146: Special Moment Frames Elevation of Building
Notes: Graphic shows: an elevation showing the North face of the building. There are seven full stories, plus a partial penthouse.

## Slide 147: Special Moment Frames Perimeter Moment Frames with RBS
System Designed
Reduced Beam Section
Notes: Graphic shows:
Detail of reduced beam flange.
Plan diagram of building with moment frames on 4 perimeter lines. Line 6 is highlighted showing that is the frame designed in the example.
The perimeter special moment frames are shown on this diagram. The seven-bay frame that acts in the E-W direction is designed in this example.

## Slide 148: Special Moment Frames
The following design steps will be reviewed:
Compute Lateral Loads
Select preliminary member sizes
Check member local stability
Check deflection and drift
Check torsional amplification
Check the column-beam moment ratio rule
Check shear requirement at panel zone
Select connection configuration
Notes: The design steps in this slide will be briefly reviewed in the subsequent slides. Additional explanation and detail is available in the FEMA 1051. A portion of the East-West frame at level two will be used to illustrate various calculations.

## Slide 149: Special Moment Frames
Building Weight:
Penthouse Roof = 94 kips
Lower Roof = 1,537 kips
Typical Floor = 1,920 kips
Total = 94 + 1,537 + 6(1,920) = 13,151 kips
Building Period:
Ta=Cthnx =(0.028) (102.3)0.8 = 1.14 sec.
T=CuTa = (1.4)(1.14)=1.596 sec. Design Base Shear:
Cs=SD1/(T/(R/I)=0.6/(1.596/(8/1))=0.047 <<< CONTROLS
Cs,min = 0.044 SDSI=0.044(1.0)(1)=0.044
V=CsW=0.047(13,151)=618 kips.
Notes: Building weights are given for the entire building.

## Slide 150: Special Moment Frames
Select preliminary member sizes – The preliminary member sizes are given in the next slide for the frame in the East-West direction. These members were selected based on the use of a 3-Dimensional model analyzed using the program ETABS. As will be discussed in a subsequent slide, the drift requirements controlled the design of these members.
Notes: Checking preliminary sizes for special moment frames.

## Slide 151: SMF Example – Preliminary Member Sizes
Notes: Graphic shows:
Elevation of frame on line 6 with column and beam member sizes (preliminary).
The preliminary member sizes were determined from the use of a structural analysis model and were based on satisfying the drift limits for this design. FEMA 1051 indicates that the drift requirements govern over the strength requirements, which is often the case for SMF designs.
Note that this example is based on Chapter 6.2 of the FEMA 1051 Examples document.

## Slide 152: SMF Example – Check Member Local Stability
bf
tf
tw
hc
OK
Upper limit:
Check beam web:
OK
Upper limit:
Check beam flange:
(W33x141 A992)
Notes: Graphic shows a wide-flange shape with flange half-width b and thickness t denoted, and the web height (hc) and thickness (tw).
The beam flange local stability limits are prescribed in the AISC Seismic specification, which is more stringent for the W shape in the SMF application. The web local stability limits are prescribed in the AISC Specification for Structural Steel Buildings. The column check is similar. Note that the provision for checking the web slenderness under combined bending and compression no longer appears in the AISC Specification for Structural Steel Buildings.

## Slide 153: SMF Example – RBS Details
c=0.20bf
b=0.75db
a=0.625bf
Notes: Graphic shows a detail of the reduced beam flange with dimensions indicated:
a distance of beginning of cut from column face
b length of cut
c width of cut on each side
The Reduced Beam Section details are shown in this slide.

## Slide 154: SMF Example – Check Deflection and Drift
Therefore, there is no vertical irregularity.
The frame was checked for an allowable story drift limit of 0.020hsx. All stories in the building met the limit. Note that the NEHRP Recommended Provisions Sec. 4.3.2.3 requires the following check for vertical irregularity:
Notes: Calculation showing drift check.

## Slide 155: SMF Example – Check Deflection and Drift
Building Satisfies Drift Limits
 | Elastic Displacement at Building Corner, From Analysis |  | Expected Displacement (=δeCd) |  | Design Story Drift Ratio |  | Allowable Story Drift Ratio
Level | de E-W (in.) | de N-S (in.) | d E-W (in.) | d N-S (in.) | D E-W/h (%) | D N-S/h (%) | D/h (%)
Level 7 | 2.92 | 3.18 | 16.0 | 17.5 | 1.2 | 1.2 | 2.0
Level 6 | 2.66 | 2.89 | 14.7 | 15.9 | 1.4 | 1.7 | 2.0
Level 5 | 2.33 | 2.47 | 12.8 | 13.6 | 1.6 | 2.0 | 2.0
Level 4 | 1.91 | 1.95 | 10.5 | 10.7 | 1.9 | 2.0 | 2.0
Level 3 | 1.41 | 1.40 | 7.76 | 7.70 | 1.8 | 1.8 | 2.0
Level 2 | 0.90 | 0.88 | 4.96 | 4.85 | 1.2 | 1.2 | 2.0
Level 1 | 0.55 | 0.52 | 3.04 | 2.89 | 1.1 | 1.1 | 2.0
1.0 in. = 25.4 mm. |  |  |  |  |  |  | 
Table 9.2-1 Alternative A (Moment Frame) Story Drifts under Seismic Loads
Notes: Calculation showing drift check. Note that drifts are checked at the building corners, although this is not required for a torsionally regular building. P-Delta effects are directly included in the computations.

## Slide 156: SMF Example – Check Torsional Amplification
The 3D analysis results, as shown in FEMA P-1051, indicate that none of the max / avg ratios exceed 1.2; therefore, torsional amplification is not required.
The torsional amplification factor is given below. If Ax < 1.0 then torsional amplification is not required. From the expression it is apparent that if max / avg is less than 1.2, then torsional amplification will not be required.
Notes: The torsional amplification equation given in the slide is described FEMA 1051. As noted, the structural analysis results indicate that torsional amplification need not be considered in this design. This is not surprising given the regularity (symmetry) of the floors and frames (placed around the perimeter.) The same regular and symmetrical building with braced frames in the core (and no moment frames) falls into the “extreme torsional irregularity” category.

## Slide 157: SMF Example – Member Design NEHRP Guide
Column Design Considerations - Columns must be adequate for:
  Combined bending and axial under basic load combinations
  Axial only under overstrength load combinations
The frame in this example is controlled by drift. So, with both strength and drift requirements satisfied, we will check the column-beam moment ratio and the panel zone shear.
Notes: The content of this slide is taken directly from FEMA 1051.

## Slide 158: SMF Example – Column-Beam Moment Ratio
where M*pc = the sum of the moments in the column above and below the joint at the intersection of the beam and column centerlines. ΣM*pc is determined by summing the projections of the nominal flexural strengths of the columns above and below the
joint to the beam centerline with a reduction for the axial force in the column.
M*pb = the sum of the moments in the beams at the intersection of the beam and column centerlines.
Per AISC Seismic Sec. E3.4a
Notes: It is permitted to take ΣM*pc = ΣZc(Fyc-Puc/Ag) (LRFD). ΣM*pb is determined by summing the projections of the expected flexural strengths of the beams at the plastic hinge locations to the column centerline. It is permitted to take ΣM*pb = Σ(1.1RyFybZb+Muv). Refer to AISC Seismic specification Sec. E3.4a for remainder of definitions.

## Slide 159: SMF Example – Column-Beam Moment Ratio
Column – W24x146; beam – W21x73
Notes: The story height for the first story is 268 in. (top of concrete to mid-depth of first floor beam and the clear height is 251.35 in. The values for the second story are 160 in. and 128.44 in. For diagrams and additional details the reader is referred to FEMA 1051 and the AISC Seismic specification.

## Slide 160: SMF Example – Column-Beam Moment Ratio
where
Mpr=CprRyFy Ze
Ze = effective Z (RBS)
Ve= 2 Mpr / L’
Sh= dist. from col. centerline to plastic hinge
For beams:
Notes: Graphic shows a free-body diagram of the beam segment between plastic hinge locations. Forces acting on the beam are:
W Distributed gravity load
Vp Shear force at each end
Mp Moments at each end
Segment length is L’
Calculations for Vp. Figure from FEMA 1051. The calculation for the factored uniform dead load, w, is given and is found to be 1.406 klf.

## Slide 161: SMF Example – Column-Beam Moment Ratio
Other ratios are also computed to be greater than 1.0
The ratio of column moment strengths to beam moment strengths is computed as:
Notes: The column-beam strength ratio for all the other stories are determined in a similar manner.

## Slide 162: SMF Example – Panel Zone Check
The AISC specification is used to check the panel zone strength. From analysis shown in the NEHRP Design Examples volume (FEMA 451), the factored strength that the panel zone at Story 2 of the frame in the EW direction must resist is 794 kips. The shear transmitted to the joint from the story above, Vc, opposes the direction of Ru and may be used to reduce the demand. Previously calculated, this is 102 kips at this location. Thus:
Ru = 794 – 102 = 692 kips.
Notes: The calculations shown use the AISC 341 methodology.

## Slide 163: SMF Example – Panel Zone Check
Since fv = 1, fvRb = 547 kips, which is less than the required resistance, 692 kips. Therefore, doubler plates are required. The required additional strength from the doubler plates is 692 – 547 = 145 kips. The plates must be at least ¼” thick as the strength of the double plates is:
Notes: The calculations shown use the AISC 341 methodology.

## Slide 164: SMF Example – Connection Configuration
Notes: The text on this slide is taken from the AISC Seismic Provisions. Connections that accommodate the required interstory drift angle within the connection elements and provide the measured flexural resistance and shear strengths specified above are permitted. In addition to satisfying the requirements noted above, the design must demonstrate that any additional drift due to connection deformation can be accommodated by the structure. The design must include analysis for stability effects of the overall frame, including second-order effects.

## Slide 165: SMF Example – Connection Configuration
Notes: The following is taken from the AISC Seismic specification. This provision specifically permits the use of prequalified connections meeting the requirements of ANSI/AISC 358, Prequalified Connections for Special and Intermediate Steel Moment Frames for Seismic Applications (AISC, 2016a) to facilitate and standardize connection design. Other prequalification panels may be acceptable but are subject to the approval of the authority having jurisdiction. Use of connections qualified by prior tests or project specific tests may also be used although the engineer of record is responsible for substantiating the connection. Published testing, such as that conducted as part of the SAC project and reported in FEMA 350 and 355, or project-specific testing may be used to satisfy this provision.

## Slide 166: Special Moment Frames Summary
Beam-to-column connection capacity
Select preliminary member sizes
Check member local stability
Check deflection and drift
Check torsional amplification
Check the column-beam moment ratio rule
Check shear requirement at panel zone
Select connection configuration
  Prequalified connections
  Testing
Notes: Review SMF requirements. FEMA 350 is the current best resource for prequalified connections. AISC will eventually become the official repository for such information. FEMA 350 is available electronically for download at the AISC ePubs site (www.aisc.org).

## Slide 167: Chapter 9: Structural Steel Design
Part 2: Design Examples:
Special Concentrically Braced Frame

## Slide 168: Special Concentrically Braced Frame Example Seven Story Office Building, Los Angeles
Multiple interior braced bays
SDS=1.0
SD1=0.6
Occupancy Category II
Seismic Design Category D
Design Parameters (Table 12.2-1)
  R=6
  Cd=5.0
  Wo=2.0
Notes: The information on the following several slides are taken from Example 6.2 (Alternate A) of the NEHRP Design Examples volume (FEMA 1051). FEMA 1051 was written based on the 2015 NEHRP Recommended Provisions. The example complies with the AISC 341.

## Slide 169: Concentrically Braced Frame Example
The following general design steps are required:
  Selection of preliminary member sizes
  Check strength
  Check drift
  Check torsional amplification
  Connection design
Notes: The general design steps for a SCBF are indicated on the slide. The load and analysis calculations, along with a summary of each of these steps are given in FEMA 1051.

## Slide 170: E-W Direction Framing and Preliminary Member Sizes
Notes: Graphic shows an elevation of the braced frame, with brace sizes indicated at every level.
This example is the same building as was considered in the SMF example, which is Example 6.2 in FEMA 1051.

## Slide 171: N-S Direction Framing and Preliminary Member Sizes
Notes: Graphic shows an elevation of the braced frame, with brace sizes indicated at every level.
This example is the same building as was considered in the SMF example, which is Example 6.2 in FEMA 1051.

## Slide 172: CBF Example
Building Weight:
Penthouse Roof = 94 kips
Lower Roof = 1,537 kips
Typical Floor = 1,920 kips
Total = 94 + 1,537 + 6(1,920) = 13,151 kips
Building Period:
Ta=Cthnx =(0.02) (102.3)0.75 = 0.64 sec.
T=CuTa = (1.4)(0.64)=0.896 sec. Design Base Shear:
Cs=SD1/(T/(R/I)=0.6/(0.896/(6/1))=0.112 <<< CONTROLS
Cs,min = 0.044 SDSI=0.044(1.0)(1)=0.044
V=CsW=0.112(13,151)=1,473 kips.
Notes: Building weights are given for the entire building.

## Slide 173: CBFF Example – Check Deflection and Drift
Building Easily Satisfies Drift Limits
Notes: Calculation showing drift check. Note that drifts are checked at the building corners, although this is not required for a torsionally regular building. P-Delta effects are directly included in the computations.

## Slide 174: CBF Example – Connection Detail
Notes: Graphic shows a detail of the connection of two braces and a beam to the column. In the detail, all three members are connected to a single gusset that is connected to the column web.
Calculation showing drift check. Note that drifts are checked at the building corners, although this is not required for a torsionally regular building. P-Delta effects are directly included in the computations.

## Slide 175: Chapter 9: Structural Steel Design
Part 2: Design Examples:
Diaphragm Design

## Slide 176: Steel Diaphragm Example
Vn =  (approved strength)
 = 0.6
For example only:
Use approved strength as 2.0 × working load in
SDI Diaphragm Design Manual
Notes: This example is not in FEMA 1051; for example only, use capacities from SDI Diaphragm Design Manual.

## Slide 177: Steel Deck Diaphragm Example
L
d
VE
VE
wE
Deck chosen:
1½”, 22 gage with welds on 36/5 pattern and 3
sidelap fasteners, spanning 5’-0”
Capacity = 450 > 417 plf
Notes: Shear in diaphragm due to dead and live loads is zero. Given the seismic load, wE=500 plf, calculate total shear at end of diaphragm; compute shear flow at end of diaphragm. Required shear capacity is shear demand divided by 2.0. Choose deck and fasteners. Fasteners and their spacing greatly affect diaphragm capacity; must carefully inspect deck welds and sidelap fasteners. Inspector needs to make sure that deck has not been burned through, and that connection has been made.
Graphic shows a plan diagram of the diaphragm with distribute loading (w), a depth d, a span L, and shear at each end Ve.

## Slide 178: Questions
Notes: Slide to initiate questions from the participants.

## Slide 179: DISCLAIMER
NOTICE: Any opinions, findings, conclusions, or recommendations expressed in this publication do not necessarily reflect the views of the Federal Emergency Management Agency. Additionally, neither FEMA nor any of its employees make any warranty, expressed or implied, nor assume any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, product or process included in this publication.
The opinions expressed herein regarding the requirements of the NEHRP Recommended Seismic Provisions, the referenced standards, and the building codes are not to be used for design purposes. Rather the user should consult the jurisdiction’s building official who has the authority to render interpretation of the code.
Any modifications made to the file represent the presenters' opinion only.