## Slide 1: REINFORCED CONCRETE STRUCTURES
Disclaimer
Notes: Title slide, consisting of an image of the cover of the data disk containing the 2015 NEHRP Recommended Seismic Provisions
This topic is the seismic design of reinforced concrete structure. During this presentation you will learn the basics of seismic design of reinforced concrete buildings.
The examples in this topic draw heavily on the examples in the FEMA P-752 Design Examples CD.

## Slide 2: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 3: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 4: Unconfined Concrete Stress-Strain Behavior
Notes: This slide presents stress-strain diagrams for unreinforced, unconfined concrete in compression.
Behavior is relatively linear up to about one-half of the maximum compressive stress. Concrete exhibits no precise yield point. Strain at maximum strength is close to 0.002 regardless of maximum stress. Lower strength concrete can have strains at crushing that exceed 0.004, however a typical design value is 0.003 at crushing. Stronger concretes are more brittle.

## Slide 5: Confinement by Spirals or Hoops
Asp
Confinement
from spiral or
circular hoop
ds
fyhAsp
fyhAsp
Forces acting
on 1/2 spiral or
circular hoop
Confinement
from square
hoop
Notes: This slide presents concrete sections confined by spirals or hoops.
Confining reinforcing can improve concrete behavior in two ways. First it can enhance strength by restraining lateral strains. Second it can increase the usable concrete compressive strain well beyond the typical value of 0.003.
This slide shows confinement in practical structural sections. Confinement is typically provided by spirals, circular hoops, or square hoops. The hatched areas in the figures may spall. Confining steel is in tension (hoop stress effect) because, due to Poisson’s effect, as the concrete is compressed in one direction, it expands in the orthogonal directions. This is shown in the center illustration. Note that hoops are not as efficient as spirals in confining concrete because the sides of the hoop can flex outward as the confined concrete expands outward. For this reason, cross ties are usually require at hoops.

## Slide 6: Confinement
Rectangular hoops
with cross ties
Confinement by
transverse bars
Confinement by
longitudinal bars
Notes: This slide shows confinement for a square column, which can be provided by transverse and longitudinal bars. The hatched areas may spall.

## Slide 7: Confined Concrete Stress-Strain Behavior
Pitch of
¼ in. dia.
spiral
Tests of
6 in. x 12 in.
cylinders
Notes: This figure presents stress-strain behavior of confined concrete section.
This slide shows the benefits of confinement on concrete behavior. Presented are stress-strain diagrams for confined concrete in compression. The specimens were 6 in. by 12 in. cylinders. Confinement was provided by spiral reinforcement. Reducing spiral pitch (or hoop spacing) increases maximum concrete stress and strain capacity (ductility).

## Slide 8: Idealized Stress-Strain Behavior of Confined Concrete
Confined Area 12” x 16”
Notes: This figure shows the idealized stress-strain behavior of confined concrete proposed by Kent and Park.
Note that the model reflects the additional strain, but not the additional strength, provided by the confinement. Another model that reflects both strength and strain gain is Scott, Park, and Priestley. This type of model can be used with the strain compatability method to predict the behavior of confined reinforced concrete.

## Slide 9: Reinforcing Steel Stress-Strain Behavior
Notes: This figure shows typical stress-strain behavior of common grades of reinforcing steel.
The most commonly used is Grade 60 which shows a distinct yield plateau and strain hardening at between 0.5% and 1% elongation. For common analysis of reinforced concrete behavior, strain hardening is ignored. For seismic design, it is important that the actual yield strain of the steel is not significantly higher than the value used in design.

## Slide 10: Reinforced Concrete Behavior
Notes: This figure shows stages of behavior of a reinforced concrete beam.
At low loads the section is uncracked and an analysis using uncracked-transformed section properties can be used to predict behavior. After the concrete cracks, the concrete on the tension side of the beam is neglected, and a cracked-transformed section analysis can be used to predict behavior. However, this method is only valid as long as both the steel and the concrete stress-strain behaviors are linear. Concrete can be assumed to have a linear stress-strain behavior up to approximately 50% of maximum concrete stress (f’c).
After the concrete stress exceeds about 50%f’c, a strain compatibility approach can be used, using a realistic concrete stress-strain model. After the steel yields, there is typically an extended plateau in which the displacement increases significantly with very little increase in applied load. A commonly used indicator of member ductility is the ratio of the displacement at ultimate to the displacement at first yield. This is known at the displacement ductility, and for seismic design in particular, bigger is better.

## Slide 11: Behavior Up to First Yield of Steel
Notes: This figure presents moment-curvature behavior of a concrete section up to first yield of steel.
To characterize section behavior, moment-curvature (M-) diagrams are often employed. This slide shows the type of strain compatibility approach that would be used to locate points on the curve up until first yield of the steel. To locate a point, first a concrete strain is selected. Then an iterative method is used in which the depth to the neutral axis is assumed and modified until internal equilibrium is achieved. The tension force is equal to the strain (based on the strain diagram with the selected concrete strain and neutral axis depth) times the area and the modulus of elasticity of the steel. The compression force is determined by integrating under the stress-position curve from the neutral axis to the extreme compression fiber, and multiplying by the width of the beam. The value of “c” is adjusted until C = T. Then the curvature is calculated as the concrete strain divided by the neutral axis depth, and the moment is the force (T or C) times the distance between the forces. This can be repeated for several selected concrete strains to determine points on the M- diagram.

## Slide 12: Behavior at Concrete Crushing
Mn = Asfyjd
Notes: This figure presents moment-curvature behavior of a concrete section at concrete crushing.
After yield but before the onset of strain hardening, the same method as presented on the previous slide can be used; however, the force in the steel will be Asfy. This method can be used for points up to the concrete crushing strain of 0.003. The Whitney stress block method is a good method to calculate the final point on the moment curvature diagram, but cannot be used for other points. Typically strain hardening is not considered in design.

## Slide 13: Typical Moment Curvature Diagram
f x 10-5 in-1
0
100
200
300
0
100
200
300
400
500
600
700
w/ strain hardening
w/o strain hardening
M, in-kip
f’c = 4 ksi
fy = 60 ksi
b = 8 in
d = 10 in
r = 0.0125
Notes: This figure shows moment-curvature diagrams for a rectangular section in flexure.
Strain hardening in the tension steel increases the final strength. A concrete strain of 0.003 corresponds to maximum strength.

## Slide 14: Influence of Reinforcement Ratio
0
100
0
1000
200
300
400
2000
3000
4000
5000
M, in-kip
f x 10-5 in-1
f’c = 4 ksi
fy = 60 ksi
b = 10 in
d = 18 in
r = 2.5%
r = 1.5%
r = 0.5%
Notes: This figure shows moment-curvature diagrams for various amounts of tension reinforcement.
As the steel percentage increases, the moment capacity also increases, but the curvature at ultimate moment capacity is decreased (less ductility). Ductile behavior is very desirable in seismic force resisting systems. A common measure of ductility is the ratio of curvature at first yield to curvature at ultimate. This is known as curvature ductility.

## Slide 15: Influence of Compression Reinforcement
f
0
0.024
400
800
1200
1600
0
0.016
0.008
1
2
3
4
5
6
7
Notes: This figure shows moment-curvature diagrams for various amounts of tension and compression reinforcement.
An increase in the compression reinforcement ratio only slightly increases moment capacity but significantly increases curvature at ultimate moment capacity (more ductility). This is because when the tension force does not change ( is constant) and neither does the compression force. With larger amounts of compression reinforcement the steel carries more of the compression, so the concrete carries less. This means the depth to the neutral axis is more shallow, so the curvature at ultimate (0.003/c) is larger. However, since C and T do not change and there is only a slight increase in the moment arm, the moment capacity only increases slightly. (Note: Curve 7 stops at about 0.025; Curve 6 continues off the graph.)

## Slide 16: Moment-Curvature with Confined Concrete
Notes: This figure presents moment-curvature behavior of a confined concrete section.
The presence of confining reinforcement can significantly increase the maximum achievable curvature. After the strain on the compression face exceeds 0.003, the cover over the confining steel will spall, however the concrete within the core will remain intact. A model such as the Kent and Park model presented earlier can be used with the strain compatibility method to calculate moments and corresponding curvatures.

## Slide 17: Moment-Curvature with Confined Concrete
Notes: This figure presents the results of the analysis of a beam, whose dimensions and reinforcing details are given on the slide.
As you can see, the addition of the confining reinforcing increases the usable curvature from just under 500 microstrain per inch to just over 1600. The Scott, Park, and Preistley model was used to model the behavior of the confined concrete. This model accounts for the increase in concrete compressive strength. In addition the compression steel was able to yield, and strain hardening was considered in the tension steel. These three factors combined to result in an increase in moment capacity from the confining steel, even though the cover concrete was lost.

## Slide 18: Plastic Hinging
Notes: This figure shows how spreading plasticity can significantly increase plastic rotation and displacements.
The curvature diagram shows a region of very high curvatures (beyond the yield curvature, y) at maximum moment and elastic response in other regions. The region of curvatures past yield curvature is known as the plastic hinge region. The irregular curvature on the “actual” curve is due to cracking.
The plastic rotation and the tip displacement can be calculated from the “actual” curvature diagram, or from the idealized curvature diagram. The idealized diagram is based on a bi-linear approximation of the moment-curvature diagram and an assumed length of the plastic hinge, lp.

## Slide 19: Strategies to Improve Ductility
Use low flexural reinforcement ratio
Add compression reinforcement
Add confining reinforcement
Notes: This slide presents strategies to improve ductility.
The previous discussion presented three strategies for improving ductility. These are summarized in this slide.

## Slide 20: Other Functions of Confining Steel
Acts as shear reinforcement
Prevents buckling of longitudinal reinforcement
Prevents bond splitting failures
Notes: This slide presents other functions of confining steel.
Confining reinforcing also has other useful functions that are presented in this slide.

## Slide 21: Structural Behavior Frames
Story Mechanism
Sway Mechanism
Notes: This figure presents failure mechanisms of frame due to lateral load, story mechanism and sway mechanism.
With an understanding of reinforced concrete member behavior, reinforced concrete systems can be designed to ensure acceptable behavior in a seismic event. We will now discuss desirable system behaviors.
The goal in design of structural frames is to size and reinforce members such that when subjected to large lateral displacements the hinges form in the beams adjacent to the columns, but the columns remain relatively undamaged. This is known as the “strong column-weak beam” approach that is illustrated in the right frame in this slide. A “weak column-strong beam” design can result in the undesirable story mechanism, also known as a soft story, that is shown in the left illustration.

## Slide 22: Story Mechanism
Notes: This slide illustrates a story mechanism with a photo.

## Slide 23: Structural Behavior - Walls
Sliding on
construction
joint
Sliding on
flexural cracks
Horizontal
tension
Flexural
failure
Notes: This figure shows types of failures in structural walls. The left figure shows a flexural failure with a plastic hinge zone at the base of the wall. The second figure shows that severe cracking necessitates that web reinforcement carries the horizontal shear force. The last two figures show types of sliding failures: sliding along full depth flexural cracks or along construction joints.
The most desirable is the flexural failure with other modes precluded. With proper detailing, the wall can exhibit good strength and ductility without excessive drift or collapse.

## Slide 24: Structural Behavior - Columns
Ultimate
yield
Moment, M, in-kip
Curvature, f, rad/in
Axial load, P, kip
0
200
400
600
800
1000
0
400
800
1600
1200
0
0.001
0.002
1.75”
bending axis
Notes: This figure presents the axial force-moment interaction curve on the left and the axial force-curvature interaction curve on the right.
In strong column-weak beam design, undesirable failures in the columns must be precluded through proper design and detailing. This slide presents the P-M curve on the left and the P-curvature curve on the right. Note that the presence of large axial loads reduces the curvature at ultimate. Axial loads above the balanced point reduce ductility of beam-columns since the reinforcing steel on the tension side of the column never yields. Confinement reinforcement improves axial ductility, but this plot shows curvature ductility, which is more important in frames. The strong column-weak beam design approach ensures that failure will initiate in ductile beams rather than in brittle columns.

## Slide 25: Influence of Hoops on Axial Strength
After spalling  Before spalling
After spalling-
P = Acore(f’c + 4 flat)
Before spalling-
P = Agf’c
Notes: This slide present influence of hoops on axial strength of a circular section.
The strength of an unconfined concrete column is the gross area times the unconfined compressive strength. After the concrete outside the spiral, hoops or ties has spalled, the strength of the column is the core area times the enhanced compressive strength. Work done in the 1920s by Richart et al. indicated that confined concrete strength is roughly the unconfined strength plus 4 times the confining pressure, flat. The goal in designing the hoops is to ensure that the strength after cover spalling is not less than the strength before spalling.

## Slide 26: Column with Inadequate Ties
Notes: The slide presents a photo showing failure of a column after an earthquake.
This photo shows a column with inadequate ties which provided almost no confinement. Olive View Hospital after the 1971 San Fernando earthquake.

## Slide 27: Well Confined Column
Notes: The slide presents a photo showing failure of a column after an earthquake.
This slide shows a column with an adequate amount of spiral confinement. After the cover spalled, the well confined core remains intact and able to carry axial loads. Olive View Hospital after the 1971 San Fernando earthquake.

## Slide 28: Hysteretic Behavior of Well Confined Column
Notes: The figure presents a chart showing hysteretic behavior of well confined column.
This type of hysteresis loop shows good performance of a column with generous confinement reinforcement. The preferred type of hysteresis loop shows only small degradation of moment strength with increased imposed drift. Also the loops remain “fat” which indicates good energy dissipation.

## Slide 29: Structural Behavior Columns
D
M1
M2
V
P
M
Mo
Mpr
Range
of P
V
V
M1
M2
L
Notes: This slide presents structural behavior of column at lateral displacement.
To ensure strong column-weak beam behavior, shear failures of columns must also be precluded. Shear is maximum in a column when the moments at each end are at their maximum, also known as the probable moment. The moment capacity of a column depends on the magnitude of the axial load. To avoid shear failures, the design should focus on the axial load that produces the largest moment capacity. The P-M interaction diagram shows this range of axial loads for an example column.

## Slide 30: Column Shear Failure
Notes: This slide presents a photo of concrete column failure after an earthquake.
This photo shows a shear failure of a bridge pier after the 1971 San Fernando earthquake.

## Slide 31: Structural Behavior Joints
Notes: This slide presents the structural behavior of beam-column joint.
Another location in frames where premature failures must be precluded is the beam-column joints. This slide shows joint actions. The left figure shows forces (stresses) imposed on a typical exterior joint, and the right shows cracks. Upon reversal of direction, perpendicular cracks form. The anchorage of the reinforcement can be compromised. The important aspects of joint design are ensuring proper bar development and precluding shear failures in the joint. This can be accomplished through proper detailing of hoop reinforcement and bar hooks.

## Slide 32: Hysteretic Behavior of Joint with Hoops
Notes: This figure shows a typical hysteresis loop for a joint with hoops. The joint shows good performance under repeated reversed loads.

## Slide 33: Hysteretic Behavior of Joint without Hoops
Notes: This figure shows a typical hysteresis loop of a joint without confining hoops.
Note the rapid deterioration of the joint.

## Slide 34: Joint Failure – No Shear Reinforcing
Notes: This figure presents a photo of beam-column joint failure after an earthquake.
This photo is of a joint failure in shear (1971 San Fernando earthquake). Note that there is NO shear reinforcement in the joint and the joint is too small. The joint can no longer transmit moments.

## Slide 35: Anchorage Failure in Column/Footing Joint
Notes: This slide presents a photo of beam-column joint failure after an earthquake.
Another type of failure which must be prevented in order to ensure ductile frame behavior is the failure of the joint between the column and the footing. This slide shows an anchorage failure of a bridge column (1971 San Fernando earthquake).

## Slide 36: Summary of Concrete Behavior
Compressive Ductility
  Strong in compression but brittle
  Confinement improves ductility by
    Maintaining concrete core integrity
    Preventing longitudinal bar buckling
Flexural Ductility
  Longitudinal steel provides monotonic ductility at low reinforcement ratios
  Transverse steel needed to maintain ductility through reverse cycles and at very high strains (hinge development)
Notes: This slide presents a summary of concrete behavior under seismic loading.
We will now review reinforced concrete behavior.
Concrete is strong in compression but brittle. Confinement improves compressive ductility by limiting transverse expansion in the concrete. As the transverse steel ties take the strain in tension, the concrete core maintains its integrity. Closely spacing the ties will limit longitudinal bar buckling and thus contribute to improved compressive ductility. Longitudinal steel provides flexural ductility at low reinforcement ratios for a single overload. Transverse steel is needed to maintain integrity of the concrete core (which carries compression and shear), and prevent longitudinal bar buckling after the cover has spalled and crossing cracks form. A relative balance of tension and compression steel aids flexural ductility. The amount of longitudinal tension steel must be limited to insure a tension-type failure mode.

## Slide 37: Summary of Concrete Behavior
Damping
  Well cracked: moderately high damping
  Uncracked (e.g. prestressed): low damping
Potential Problems
  Shear failures are brittle and abrupt and must be avoided
  Degrading strength/stiffness with repeat cycles
    Limit degradation through adequate hinge development
Notes: This slide presents a summary of concrete behavior under seismic loading.
The level of damping in concrete structures depends on the amount of cracking. It is important to avoid potential problems in concrete structures: Shear failures in concrete are brittle and abrupt and must be avoided; repeated loadings degrade strength and stiffness as concrete cracks and steel yields. Degradation can be limited by assuring adequate hinge development.

## Slide 38: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 39: Reference Standards
16
Notes: This slide shows photos of the covers of reference standards ASCE 7-16 and ACI 318-14

## Slide 40: Modifications to Reference Standards
Notes: This slide shows cover of FEMA P-1050 and proposed modifications to ASCE 7 Section 14.2.

## Slide 41: Context in NEHRP Recommended Provisions
Provisions  ASCE 7-16  ACI 318-14
ASCE 7-16 for Concrete
Structural design criteria: Chap. 12
Structural analysis procedures: Chap. 12
Design of concrete structures: Sec. 14.2
Provisions modifications to ASCE 7-10
ASCE 7-16 modifications to ACI 318-14
Notes: This slide describes the context in NEHRP Recommended provisions to ASCE 7 and ACI 318-14.
The 2015 NEHRP Recommended Provisions provides the basis of modifications in ASCE 7-16 from ASCE 7-10. ASCE 7-16 references ACI 318-14 for concrete structures. Required strength (demand) is determined from ASCE 7 Chapter 12, and provided strength (capacity) is calculated using ASCE 7 Section 14.2 which references ACI 318.

## Slide 42: Reference Standards
ASCE 7-16: Defines systems and classifications Provides design coefficients ACI 318-14: Provides system design and detailing requirements consistent with ASCE 7-16 system criteria Modified by ASCE 7-16
Notes: This slide provides summary of the scope of the two main reference standards

## Slide 43: Seismic-Force-Resisting Systems
Moment Frames
Cast-in-Place
Special
Intermediate
Ordinary
Precast
Special
Shear walls
Cast-in-Place
Special
Ordinary
Detailed plain
Ordinary plain
Precast
Intermediate
Ordinary
Dual Systems
Notes: The figure shows two common seismic-force-resisting systems using reinforced concrete, moment frames and structural walls.
This slides presents a list of seismic-force-resisting systems included in ACI 318-14.
The two common seismic-force-resisting systems using reinforced concrete are moment frames and structural walls. A combination of structural walls and moment frames can be considered a dual system when certain criteria are met.
ASCE 7 Section 12.2 presents design coefficients and system limitations for various Seismic Design Categories. Precast walls can be used, however they will not be addressed in detail in this session.
The system classifications relate to detailing requirements and associated the ductility of the structural systems. The system ductility relates to the basic reinforced concrete behavior covered previously.

## Slide 44: Use of Reference Standards
ACI 318
  Chapter 18, Earthquake-Resistant Structures
ASCE 7-16 and Provisions Section 14.2
  Modifications to ACI 318
  Detailing requirements for concrete piles
Provisions supersede ASCE 7-10 modifications
Notes: This slide presents use of reference standards.
ACI 318-14 Chapter 18 contains all the design provisions for earthquake-resistant structures. Provisions and ASCE 7 Section 14.2 presents some modifications to ACI 318 Chapter 18 as well as some additional reinforced concrete structure requirements. This presentation will not cover the precast concrete provisions in any detail.

## Slide 45: Detailed Modifications to ACI 318
Wall piers and wall segments
Members not designated as part of the LRFS
Columns supporting discontinuous walls
Intermediate precast walls
Plain concrete structures
Anchoring to concrete
Foundations
Acceptance criteria for validation testing of special precast walls
Notes: This slide presents modifications to ACI318 made by the Provisions and ASCE 7.
This list includes the main modifications to ACI 318 that are contained in the Provisions and ASCE 7. Most of these are not addressed in more detail in this session.

## Slide 46: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 47: Design Coefficients Moment Resisting Frames
Seismic Force Resisting System | Response Modification Coefficient, R | Deflection Amplification Factor, Cd
Special R/C Moment Frame | 8 | 5.5
Intermediate R/C Moment Frame | 5 | 4.5
Ordinary R/C Moment Frame | 3 | 2.5
Notes: This slide presents the design coefficients presented ASCE 7 Table 12.2-1.
These tables also present system limitations and height limits by Seismic Design Category (not shown in slides).

## Slide 48: Design Coefficients Structural Walls (Bearing Systems)
Seismic Force Resisting System | Response Modification Coefficient, R | Deflection Amplification Factor, Cd
Special R/C Structural Walls | 5 | 5
Ordinary R/C Structural Walls | 4 | 4
Intermediate Precast Structural Walls | 4 | 4
Ordinary Precast Walls | 3 | 3
Notes: This slide presents the coefficients for structural walls that are part of a bearing wall system.

## Slide 49: Design Coefficients Structural Walls (Frame Systems)
Seismic Force Resisting System | Response Modification Coefficient, R | Deflection Amplification Factor, Cd
Special R/C Structural Walls | 6 | 5
Ordinary R/C Structural Walls | 5 | 4.5
Intermediate Precast Structural Walls | 5 | 4.5
Ordinary Precast Walls | 4 | 4
Notes: This slide presents the coefficients for structural walls that are part of a building frame system.

## Slide 50: Design Coefficients Dual Systems with Special Frames
Seismic Force Resisting System | Response Modification Coefficient, R | Deflection Amplification Factor, Cd
Dual System w/ Special Walls | 7 | 5.5
Dual System w/ Ordinary Walls | 6 | 5
Notes: This slide presents the coefficients for dual systems that include a special moment resisting frame.

## Slide 51: General Requirements
Seismic Design Category | ACI 318-14 Requirements | Description
B | Sec. 18.2.1.3 Sec. 18.2.2 | Analysis and proportioning
C | Sec. 18.2.1.4 Sec. 18.2.2 Sec. 18.2.3 | Analysis and proportioning Anchoring to concrete
D, E & F | Sec. 18.2.1.5 Sec. 18.2.2 through 18.2.8 Sec. 18.12 through 18.14 | Analysis and proportioning Anchoring to concrete Diaphragms, foundations, & non LRFS members
Notes: This slide illustrates some general requirements for concrete buildings based on Seismic Design Category and independent of specific lateral force resisting system.
Consistent throughout the Provisions the design scope is more detailed for higher Categories.

## Slide 52: Moment Frames
Seismic Design Category | Minimum Frame Type | ACI 318-14 Requirements
B | Ordinary | Chapters 1-17 and 19-26 Sec. 18.3
C | Intermediate | Sec. 18.4
D, E and F | Special | Secs. 18.2.3-18.2.8 and 18.6-18.8
Notes: This slide presents ACI 318-14 requirements for moment frames.
The Provisions define three types of frames: ordinary, intermediate, and special. Ordinary moment frames have very few requirements in ACI 318 Chapter 18. For the most part, they are designed in accordance with the non-seismic chapters of ACI 318. Intermediate moment frames must meet requirements of ACI 318 section 18.4 which are more stringent detailing than for ordinary frames but less severe than for special frames). The overall level of ductility is between Ordinary and Special.
Special moment frames must meet detailed requirements contained in various sections of ACI 318, Chapter 18, including detailing to ensure ductility, stability, and minimum degradation of strength during cyclic loading. A review of ASCE 7 Table 12.2-1 (excerpts shown on the previous slides) shows that the values of R and Cd reflect the expected behavior of the various types of moment frames. The Seismic Design Category (SDC) dictates what type of frame may be used. In SDC B, ordinary frames may be used. Intermediate frames are required (at a minimum) in SDC C (although a special frame may be more economical because the higher R will mean lower design forces). For SDCs D, E and F, frames must be special.
There are exceptions to the limitations on type of frame, especially for nonbuilding structures of limited height.

## Slide 53: Reinforced Concrete Structural Walls
Seismic Design Category | Minimum Wall Type | ACI 318-14 Requirements
B and C | Ordinary | Chapters 1-17 and 19-26 (unless required by 18.2.1.3 or 18.2.1.4)
D, E and F | Special | Secs. 18.2.3-18.2.8 and Sec. 18.10
Notes: This slide presents ACI 318-14 requirements for reinforced concrete structural walls.
For reinforced concrete structural walls there are just two main types: Ordinary (not Chapter 18) and Special (Chapter 18). Plain concrete walls, designed per Chapter 14, are permitted in SDC B for some circumstances.

## Slide 54: Precast Concrete Structural Walls
Seismic Design Category | Minimum Wall Type | ACI 318-14 Requirements
B | Ordinary | Chapters 1-17 and 19-26
C | Intermediate | Sec. 18.5
D, E and F | Special | Secs. 18.2.3-18.2.8; Sec. 18.11
Notes: This slide presents ACI 318-14 requirements for precast concrete structural walls.
Precast structural walls are also allowed to be part of the seismic force resisting system. The intent for special precast walls is that they qualify for the same design parameters as the special cast-in-place wall. Unlike cast-in-place concrete walls, there is an Intermediate classification for precast concrete walls.
ACI 318-14 contains a section on special precast walls (Section 18.11); however, the system is not presented in ASCE 7 Table 12.2-1. There is a large section in Section 14.2 of the Provisions, that presents acceptance criteria for special precast structural walls based on validation testing. This presentation does not include detailed information on precast walls.

## Slide 55: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 56: Performance Objectives
Special Moment Frames
  Strong column
    Avoid story mechanism
  Hinge development
    Confined concrete core
    Prevent rebar buckling
    Prevent shear failure
  Member shear strength
  Joint shear strength
  Rebar development and splices (confined)
Notes: This slide presents Performance Objectives of Special Moment Frame system.
The requirements of Special Moment Frames in ACI 318 Chapter 18 are intended to ensure the performance objectives listed on this slide. The strong column-weak beam design avoids forming a mechanism in a single story (the story mechanism presented earlier). Adequate hinge development is needed for ductility and is accomplished by the use of transverse reinforcement which confines the concrete core and prevents rebar buckling. Shear strength must be adequate to avoid abrupt failures in members and joints. Requirements for rebar anchorage and splicing (such as 135 degree hooks) are intended to maintain the integrity of the design.

## Slide 57: Performance Objectives
Intermediate Moment Frames
  Avoid shear failures in beams and columns
  Plastic hinge development in beams and columns
  Toughness requirements for two-way slabs without beams
Ordinary Moment Frames
  Minimum ductility and toughness
  Continuous top and bottom beam reinforcement
  Minimum column shear failure protection
Notes: This slide presents Performance Objectives of Special Moment Frame system (continued).
Intermediate frames have less ductility, with detailing requirements to prevent the most significant types of failures, namely shear failures, and they requirements provide a moderate level of ductility and toughness.
Ordinary moment frames have very few detailing requirements, only those associated with minimal ductility.

## Slide 58: Special Moment Frames
General detailing requirements
Beams
Joints
Columns
Example problem
Notes: This slide provides a summary of the design features of Special moment frames that will be covered in this section.

## Slide 59: Frame Mechanisms “strong column – weak beam”
Story mechanism
Sway mechanism
Notes: This figure presents failure mechanisms of frame due to lateral load, story mechanism and sway mechanism.
This slide presents failure mechanisms of frame due to lateral load.
As discussed previously, strong column-weak beam design is required for special moment frames. This slide reiterates the advantages. For a system with weak columns, a mechanism is created when the columns of only one story reach their flexural capacities (less dissipation of seismic energy prior to collapse). For a system with strong columns and weak beams, a mechanism is created when ALL beams on ALL stories yield (much more seismic energy dissipated prior to collapse).

## Slide 60: Required Column Strength
M
M
M
M
nc1
nc2
nb2
nb1
Notes: This figure presents the required column strength with respect to beam strength.
To ensure that the beams develop plastic hinges before the columns, the sum of the flexural strengths of the columns at a joint must exceed 120% of the sum of the flexural strengths of the beams. This requirement protects against premature development of a story mechanism, but due to the realities of dynamic response, it does not assure a full building mechanism.

## Slide 61: Hinge Development
Tightly Spaced Hoops
  Provide confinement to increase concrete strength and usable compressive strain
  Provide lateral support to compression bars to prevent buckling
  Act as shear reinforcement and preclude shear failures
  Control splitting cracks from high bar bond stresses
Notes: This slide presents information regarding hinge development.
It is also important in this type of system to ensure proper hinge development. The hinges must be able to form and then undergo large rotations and load reversals without significant reduction in strength. In this way, plasticity and hinging will be able to spread throughout the frame. Tightly spaced hoops are required to ensure proper hinge development and behavior. Some of the functions of the hoops are presented in this slide.

## Slide 62: Hinge Development
Before
spalling
After
spalling
Notes: This figure presents some of the mechanics of hinge development, before spalling and after spalling.
Prior to spalling, the familiar stress diagram is present, with tension in the bottom steel, compression in a roughly parabolic distribution in the concrete, and some compressive stress in the top steel. Upon spalling, the stress distribution changes, The compression block of the concrete moves lower in the cross section, and the stresses in the compression steel are greatly increased. To maintain section integrity, material component failures must be avoided. Concrete crushing and compression bar buckling can be prevented by transverse reinforcement. Closely spaced hoop steel limits lateral strain in the concrete and allows greater useful strains in the concrete and hence improved ductility. Proper spacing of hoops also prevents longitudinal bar buckling.

## Slide 63: Hinge Development
Bidirectional cracking
Spalled cover
Notes: The figure shows that under reverse load applications, hinge development affects both the top and bottom faces of beams. This leads to bidirectional cracking and spalling of cover on the top and bottom of the beam.
This slide presents some of the mechanics of hinge development (continued).

## Slide 64: ACI 318, Overview of SMF: Beam Longitudinal Reinforcement
Splice away from hinges and
enclose within hoops or spirals
Joint face Mn+ not less than 50% Mn-
Min. Mn+ or Mn- not less than
25% max. Mn at joint face
At least 2 bars continuous
top & bottom
Notes: This figure presents the beam longitudinal reinforcement requirements per ACI 318. The top figure shows the reinforcement ratio limits insure a tension controlled failure mode in bending and reduce congestion of reinforcing steel. Continuous bars in the top and bottom are required due to reversal of seismic motions and variable live load. The bottom two figures show that splice locations and transverse reinforcement are specified because lap splices are unreliable and cover concrete will spall.

## Slide 65: ACI 318, Overview of SMF: Beam Transverse Reinforcement
Longitudinal bars on perimeter
tied as if column bars
Stirrups elsewhere, s  d/2
2h
min
Closed hoops at hinging regions
with “seismic” hook
135º hook, 6dh  3” extension
Maximum spacing of hoops:
d/4 6db 6”
Notes: The top figure show the hoop design requirements and the bottom figure shows the spacing requirement of hoops.
This slide shows additional beam longitudinal reinforcement requirements per ACI 318.
Seismic hooks have special detailing requirements to ensure that the hoops do not open after the cover spalls. The maximum hoop spacing ensure adequate confinement of the concrete core and adequate lateral support of the compression reinforcing bars. However, maximum spacing may be dictated by shear design. To prevent longitudinal bar buckling, the requirements for tying compression reinforcing steel also apply to the bars in the expected plastic hinge region (over a distance equal to twice the beam depth from the face of the support).

## Slide 66: ACI 318, Overview of SMF: Beam Shear Strength
analysis
by
V
e
³
20
Mpr2
Mpr1
Ve1
Ve2
1.2D + 1.0L + 0.2S
n
f
A
Pu
and
V
2
1
'
c
g
e
<
>
then Vc = 0
If earthquake-induced
shear force
Notes: The figures shows a beam under uniform distributed load.
This slide presents the beam shear strength requirements per ACI 318.
Shear demand is based on the maximum probable flexural strength of the beam. The probable flexural strength is based on the assumption that the flexural reinforcement will achieve a stress of 1.25 times yield. To determine the expected shear from seismic effects, the probable moment strength is applied at each end of the beam and the resulting shear is calculated. This shear demand is added to the demand from gravity loads. For beams (small axial load), concrete shear strength is neglected when the earthquake-induced shear force ((Mpr1+Mpr2)/n) represents one-half or more of the design shear strength of the beam.

## Slide 67: ACI 318, Overview of SMF: Beam-Column Joint
C
T
Vcol
Vj
Notes: The figure presents free body diagram at a beam-column joint.
The design shear for joints is determined from the maximum probable flexural capacities of the beams framing into the joint and the shear in the columns. The column shear is also based on the maximum probable flexural strength of the beams. In this way, the joint shear is directly related to the amount of reinforcement in the beams framing into the joints.

## Slide 68: ACI 318, Overview of SMF: Beam-column Joint
Vn often controls size of columns
Coefficient depends on joint confinement
To reduce shear demand, increase beam depth
Keep column stronger than beam
Notes: This slide presents nominal shear strength of a beam-column joint.
Joint shear strength is based on the area of the joint, which is usually the area of the column. Nominal joint shear stress is a function of confinement. More confinement implies higher permissible shear stress. The joint shear strength often controls the sizes of the framing members. If additional joint shear strength is required, usually the column size is increased. If beam depth is increased to reduce joint shear, care must be taken to maintain the strong column-weak beam design.

## Slide 69: ACI 318, Overview of SMF: Column Longitudinal Reinforcement
Mnc based on factored axial force,
consistent with direction of lateral forces
(strong column-weak beam)
M
M
M
M
nc1
nc2
nb2
nb1
Notes: This figure presents the column longitudinal reinforcement requirements per ACI 318.
The limits on reinforcement ratio provide a sizeable difference between cracking and yielding moments and prevent steel congestion. When fulfilling the strong column-weak beam rule, recognize that moment capacity varies with axial load.

## Slide 70: ACI 318, Overview of SMF: Column Transverse Reinforcement at Potential Hinging Region
nl: number of longitudinal bars that are laterally supported by the corner of hoops or by seismic hooks
Notes: 508 note: The minima for the area of transverse reinforcement is based on providing adequate confinement of the core concrete to ensure that the strength of the column after the cover has spalled equals or exceeds the strength of the column prior to cover loss. New requirements (equations (c) and (f)) have been added to ACI 318 -14 which are applicable to columns with high compression or high strength concrete.

## Slide 71: ACI 318, Overview of SMF: Column Transverse Reinforcement at Potential Hinging Region
Spacing shall not exceed the smallest of:
b/4 or 6 db or so (4” to 6”)
Distance between longitudinal bas supported by hoops or cross ties, hx  14”
hx
hx
Notes: This figure presents the column transverse reinforcement spacing requirements per ACI 318.
Spacing of the transverse reinforcement (so) is limited to prevent longitudinal bar buckling. The distance between the legs of rectangular hoops (hx) is limited because the hoops try to become circular (bend outward due to lateral expansion of confined concrete) after the concrete cover spalls.

## Slide 72: ACI 318, Overview of SMF: Potential Hinge Region
For columns supporting stiff members such as walls, hoops are required over full height of column if
For shear strength- same rules as beams (concrete shear strength is neglected if axial load is low and earthquake shear is high)
Lap splices are not allowed in potential plastic hinge regions
Notes: 508 note: This slide presents other requirements for columns per ACI 318.
Columns under discontinued stiff members tend to develop considerable inelastic response (thus more transverse reinforcement is required). The shear design is similar to that for beams with the demand calculated based on the maximum probable strengths of the beams framing into the columns; shear strength of concrete is neglected if axial load is low and earthquake-induced shear is more than 50% of the maximum required shear strength within the plastic hinge region.

## Slide 73: Splice in Hinge Region
Terminating
bars
Notes: This slide shows a failure at the base of a column that had splices in the hinge region. (Building C, Adapazari, Turkey, 1999 Izmit earthquake.)

## Slide 74: ACI 318, Overview of SMF: Potential Hinge Region
Notes: This slide presents the definition of the potential hinge region, where the highest level of confinement is required for columns per ACI 318.
The hinge region is not to be assumed less that the largest of the three values.

## Slide 75: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 76: Performance Objectives
Special R/C structural walls
  Resist axial forces, flexure and shear
  Boundary members
    Where compression stress/strain is large, maintain capacity
  Development of rebar in panel
  Ductile coupling beams
Ordinary R/C structural walls
  No seismic requirements, Ch. 18 does not apply
Notes: This slide presents performance objectives of structural walls.
Design of structural walls for seismic resistance includes designing to resist axial forces, flexure, and shear. Special boundary confinement is required at the ends of walls where the maximum compressive stress associated with flexural and axial loads are high.
In additional to structural walls, ACI 318 provides detailing requirements for coupling beams.
Since ACI 318 Chapter 18 does not have any seismic provisions for Ordinary structural walls, they are not covered in this presentation.

## Slide 77: Design Philosophy
Flexural yielding will occur in predetermined flexural hinging regions
Brittle failure mechanisms will be precluded
  Diagonal tension
  Sliding hinges
  Local buckling
  Shear failures in coupling beams
Notes: This slide presents design philosophy of structural walls.
The design philosophy for walls is to ensure a ductile, flexural failure mechanism and preclude all brittle mechanisms.

## Slide 78: ACI 318, Overview of Special Walls: General Requirements
Shear plane, Acv =
web thickness x
length of wall
 = perpendicular
to shear plane
t = parallel to shear plane
Notes: This slide presents some of the ACI 318 notation for dimensions and reinforcing ratios in special structural walls.

## Slide 79: ACI 318, Overview of Special Walls: General Requirements
 and t not less than 0.0025 unless
then per Sec.11.6
Spacing not to exceed 18 in.
Reinforcement contributing to Vn shall be continuous and distributed across the shear plane
Notes: This slide presents some of the minimum reinforcing requirements for special structural walls.

## Slide 80: ACI 318, Overview of Special Walls: General Requirements
Two curtains of reinforcing required if:
Design shear force determined from lateral load analysis
Notes: This slide presents more requirements for special structural walls.

## Slide 81: ACI 318, Overview of Special Walls: General Requirements
Shear strength:
Walls must have reinforcement in two orthogonal directions
c = 3.0 for hw/w1.5
c = 2.0 for hw/w2.0
Linear interpolation between
Notes: This slide presents requirements for shear strength of the special structural walls.
The equation for shear strength of walls recognizes the higher shear strength of walls with high shear-to-moment ratios. For stout walls,  shall not be less than t.

## Slide 82: ACI 318, Overview of Special Walls: General Requirements
P
M
For axial load and flexure, design like a column to determine axial load – moment interaction
Notes: The figure shows a wall under load P and moment M.
This slide presents design requirements of special wall considering axial load –moment interaction.
To determine the required longitudinal reinforcement, the wall is treated like a column. An interaction diagram can be developed for the selected reinforcing layout, and checked against combinations of axial load and moment as determined from analysis.

## Slide 83: ACI 318, Overview of Special Walls: Boundary Elements
Extra confinement and/or
longitudinal bars at end
Widened end with confinement
For walls with a high
compression demand
at the edges – special
boundary elements
are required
Notes: This figure presents boundary element requirements in a structural walls.
If there is a high compressive strains or stresses at the ends of the structural wall, special boundary element detailing is required. A boundary element is a portion of the wall which is well confined. Widening of the wall is not required, though it can be beneficial, especially in reducing the length of the boundary element or reducing the vertical extent of the boundary element. More on this later….

## Slide 84: ACI 318: Overview of Special Walls Boundary Elements
Two options for determining need for boundary elements
Strain-based: Determined using wall deflection and associated wall curvature
Stress-based: Determined using maximum extreme fiber compressive
Notes: This slide presents the two possible methods for checking if boundary elements are required.
There is a strain-based method and a stress-based method. Both are described in the following slides.

## Slide 85: ACI 318, Overview of Special Walls: Boundary Elements—Strain
Boundary elements are required if:
u = Design displacement
c = Depth to neutral axis from strain
compatibility analysis with loads
causing u
Notes: This slide presents one of the two methods ACI 318 presents to check if boundary elements are required.
This method uses strains associated with structural wall curvature to determine if boundary element confinement is required.

## Slide 86: ACI 318, Overview of Walls: Boundary Elements—Strain
Where required, boundary elements must extend up the wall from the critical section a distance not less than the larger of:
w or Mu/4Vu
Notes: This slides presents requirements for extension of boundary elements along the height of wall.
If the strain-based method is used to determine if a boundary element is required, the method presented on this slide is used to determine at what height up the wall the boundary element can be terminated.

## Slide 87: ACI 318: Overview of Walls Boundary Elements—Stress
Boundary elements are required where the maximum extreme fiber compressive stress calculated based on factored load effects, linear elastic concrete behavior and gross section properties, exceeds 0.2f’c
Boundary element can be discontinued where the compressive stress is less than 0.15f’c
Notes: This slide presents the second possible method for checking if boundary elements are required—the stress-based method.
This method has a different way to determine at what point on the wall the boundary element can be discontinued.

## Slide 88: ACI 318: Overview of Walls Boundary Elements—Detailing
Boundary elements must extend horizontally not less than the larger of c/2 or c-0.1w
Width of boundary elements, b > hu/16 or 12”
In flanged walls, boundary element must include all of the effective flange width and at least 12 in. of the web
Transverse reinforcement must extend into the foundation
Horizontal reinforcement shall extend into the core of boundary and anchored to develop fy.
Notes: This slide presents detailing requirements of boundary elements.
Regardless of method used to determine where boundary elements are required, the detailing is the same as indicated on this slide. The factor c is the maximum depth to the neutral axis using any of the governing load combinations.

## Slide 89: ACI 318: Overview of Walls Coupling Beams
Standard or diagonal
Other cases
Reinforce with 2 intersecting groups of diagonal bars
Design as Special Moment Frame beam
Requirements based on aspect ratio and shear demand
Notes: This slide illustrates the basic design of coupling beams in accordance with ACI 318.
Beams with higher aspect rations can be designed as standard ductile beams. However, if the aspect ratio is smaller and shear demand high, the beam must be reinforced with diagonal bars.

## Slide 90: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 91: Members Not Part of LFRS
In frame members not designated as part of the lateral-force-resisting system in regions of high seismic risk:
  Must be able to support gravity loads while subjected to the design displacement
  Transverse reinforcement increases depending on:
Forces induced by drift
Axial force in member
Notes: This slides presents requirements for members not part of lateral force resisting system.
ACI 318 has provisions to ensure that gravity members can accommodate the expected seismic drift while maintaining their ability to support the design gravity loads.

## Slide 92: Diaphragms
Check:
Shear strength and reinforcement (min. slab reinf.)
Chords (boundary members)
- Force = M/d Reinforced for tension
(Usually don’t require boundary members)
Load from analysis in accordance
With design load combinations
Collectors, if req’d to transfer force
from diaphragm to structural walls
Shear walls
Diaphragm
Notes: This figure shows a view of a diaphragm.
The slide shows where collectors might be needed to transfer forces from a long diaphragm into a narrow structural wall. The design load is to be from seismic analysis in accordance with the design load combinations. Slab reinforcement is based on shear stress or slab reinforcement minima (same as for slender structural walls). The chord (boundary element) of a diaphragm is designed to resist tension and compression of M/d. Diaphragms rarely require confined chords. There are also special considerations for topped and untopped precast diaphragms.

## Slide 93: Struts and Trusses: Performance Objectives
All members have axial load (not flexure), so ductility is more difficult to achieve
Full length confinement
Notes: This slide presents performance objectives of strut and truss systems.
Truss systems of reinforced concrete are rarely used. Ductility, usually developed in flexure, is difficult to achieve. Every member in a truss is axially loaded; therefore, every member is designed and reinforced as a column. Full height confinement is used in all members. Anchorage is extremely important to assure adequate post yield response.

## Slide 94: Precast Concrete: Performance Objectives
Ductile connections
Inelastic action at field splice
Strong connections
Configure system so that hinges occur in factory cast members away from field splices
Field connections
must yield
Field connections
at points of low
stress
Notes: The top left figure shows field connections at points of low stress, and top right figure shows the filed connections must yield.
This slide presents performance objectives of precast concrete systems.
Frames can be based on one of two basic modes of behavior in precast buildings:
Precast that emulates monolithic construction used for frames (strong connections). For this type of system, field connections are made at points of low stress, and the hinges will occur in factory cast members, not field splices.
Jointed precast with ductile connections. For this type of system, yielding occurs in the field connections.
In the NEHRP Provisions, acceptance of special precast structural walls is based on validation testing.

## Slide 95: Quality Assurance: Rebar Inspection
Special inspection
  Rebar placement
  Prestressing tendon placement, stressing, grouting
  Concrete placement
Testing
  Rebar (ratio of yield to ultimate)
  Concrete
Notes: This slide presents quality assurance requirements in ASCE 7.
Quality assurance is covered in ASCE 7 Chapter 11A. However, this chapter is often not adopted by the local building code, so the QA requirements are often those contained in the model building code.
A quality assurance plan is generally required for most seismic force resisting systems.
This slide contains a general list of the types of testing and inspection required for concrete buildings.

## Slide 96: Topic Overview
Concrete and reinforcement behavior
Reference standards
Requirements by Seismic Design Category
  Moment resisting frames
  Shear walls
Other topics
Design Examples from FEMA P-751
Notes: This slide provides the outline of this presentation.
The first part addresses general behavior of reinforced concrete both individual members and systems, in particular as it relates to earthquake loading and ductility. This section does not directly relate to the Provisions can be shortened or eliminated based on the length or focus of the presentation.
The second and third parts cover the requirements for concrete structures based on the Provisions, ASCE 7, and primarily ACI 318.
The fourth part covers the requirements for concrete moment frames, especially Special moment frames, and includes the ACI 318 requirements use the concrete example problem to illustrate the concepts.
The fifth part covers the requirements for concrete structural walls, in particular special structural walls. The concrete example problem is again used to illustrate the main design features.
The final section addresses other design and construction topics including diaphragms and quality assurance.

## Slide 97: Special Moment Frame Example
5 @ 20’ = 100’
7 @ 30’ = 210’
A
A’
B
C
C’
D
1
2
3
4
5
6
7
8
N
Typical Floor Plan
Located in Berkeley, California
12-story concrete building
N-S direction: SMF
E-W direction: dual system
Seismic Design Category D
Modal Analysis Procedure
Notes: The figure shows a typical floor plan.
This slide includes descriptions on the design example of special moment frame.
We will now work through a design example. This moment frame example is found in Chapter 7 of the NEHRP Recommended Provisions: Design Examples (FEMA P-751). In the North-South direction, the seismic force resisting system is a special moment frame. In the East-West direction, it is a dual system with moment resisting frames on Column Lines 1, 2, 7, and 8, and structural walls between Column Lines B and C along Lines 3-6. Note that Column Lines 1 and 8 have 6 columns while Column Lines 2 and 7 have only 4 columns. The example will focus on beams, columns and joints in the frame on Column Line 1.

## Slide 98: Frame Elevations
Grid Lines 2 and 7
Grid Lines 3 to 6
Notes: This figure shows the elevation views of the frames on Column Lines 2 and 3.
Note the structural wall on Column Lines 3 to 6.
The concrete used in the majority of the building is normal-weight concrete with f’c = 5,000 psi. To perform the analysis, initial member sizes were estimated then adjusted as the design process required.

## Slide 99: Story Shears: E-W Loading
Notes: This figure presents the story shears on Frames Lines 1, 2, and 3.
All of the structural wall lines (grid 3-6 are similar to grid 3). Note the locations where story shears are negative for Frames 2 and 3. Also note that the frame line with the structural wall attracts the greatest portion of the seismic shear.
Note also that the story shears are the greatest at Frame 1 at Level 7 due to the interaction between the frames and walls. Therefore, this example focuses on the elements at Level 7.

## Slide 100: Seismic Analysis: Dual Systems
25% forces w/o
structural wall
100% forces with
structural wall
For dual systems, moment frame must be designed to resist at least 25% of design seismic forces (ASCE 7, Sec. 12.2.5.1)
Notes: The figure shows the story shear with two cases, 100% forces with structural wall, and 25% forces without structural wall.
This slide presents requirement and story force profiles of dual system.
ASCE 7 Section 12.2.5.1 requires that for dual systems the moment frame without walls must be capable of resisting at least 25% of the design forces. The building was reanalyzed with the walls removed and 25% of the equivalent seismic forces applied. This slide compares story shears from the original analysis with the 25% rule. Note that this rule controls the design for the ground level frames.

## Slide 101: Layout of Reinforcement
30”
24”
32”
29.5”
28.5”
4
#4 stirrup
#8 bar, assumed
Notes: This figure shows the layout of reinforcement for beams intersecting at Column Line 4 for Frame 1. The typical beams are 24 inches wide by 32 inches deep.
Note the different values of d for beams in each direction.

## Slide 102: Design Strengths
Design Aspect | Strength Used
Beam flexure | Design strength
Beam shear | Maximum probable strength
Beam-column joint | Maximum probable strength
Column flexure | 1.2 times nominal beam strength
Column shear | Maximum probable strength
Notes: This slide reviews how strengths are calculated for various aspects of design.
Maximum probable strength is used when a higher strength than the design strength causes more severe effects. Column strength is modified by the strong column-weak beam rule.

## Slide 103: Bending Moment Envelopes: Frame 1 Beams, 7th Floor
Notes: This figure shows the bending moment envelopes for beams in Frame 1 at Level 7.
The structure and the moment envelopes are symmetric about the centerline.
The combinations are:
1.2D + 1.6L
1.2D + 1.0E + 0.5L
0.9D + 1.0E
With E defined as QE ± 0.2SDSD with SDS=1.1 and =1.0. QE is the effect from horizontal seismic forces.

## Slide 104: Beam Reinforcement: Longitudinal
Design for Negative Moment at the Face of the Interior Support (Grid A’):
Mu = 1.46(-602) + 0.5(-278) + 1.0(-3,973) = -4,976 inch-kips
One #7 bars in addition to the four #8 bars required for minimum steel:
As = 4(0.79) + 1(0.60) = 3.76 in^2
a = 3.76 (60)/[0.85 (5) 24] = 2.21 inches
FMn = 0.9(3.76)60(29.5 – 2.21/2) = 5,765 inch-kips
> 4,976 inch-kips
.
Notes: This slide presents design of longitudinal reinforcement in the beam.
First the beam longitudinal (top) reinforcement is calculated. We will provide three (must be at least two) continuous bars top and bottom. Additional top bars are provided as necessary for moment capacity. The reinforcement ratio is checked against the ACI 318 limits for maximum and minimum

## Slide 105: Beam Reinforcement: Longitudinal (continued)
Design for Positive Moment at Face of Interior Support (Grid A’):
Mu = [-0.64(602)] + [1.0(3,973)] = 3,593 inch-kips
Four #8 bars similar to the exterior support location are adequate by inspection.
Notes: This slide presents design of longitudinal reinforcement in the beam (continued).
Next the reinforcement for positive moment at the face of the column is determined. Note that the calculated positive moment demand is greater than half of the negative moment demand. The larger of these two values governs design. For calculation of positive moment capacity the effective width of the beam, since the compression block is within the slab, includes one twelfth of the span length. This is from the effective flange width provisions of ACI 318 Section 6.3.2. In this case the minimum reinforcement is adequate.

## Slide 106: Beam Reinforcement: Longitudinal (continued)
Minimum of two bars continuous top and bottom: | OK (three #8 bars continuous top OK (four #8 bars continuous top and bottom)
Positive moment strength greater than 50 percent negative moment strength at a joint: | OK (at all joints)
Minimum strength along member greater than 0.25 maximum strength: | OK (As provided = four #8 bars is more than 25 percent of reinforcement provided at joints)
Check additional requirements:
Notes: This slide presents design of longitudinal reinforcement in the beam (continued).
In addition to the computed strength requirements and minimum reinforcement ratios described in the previous slides, the final layout of reinforcing steel also must satisfy the additional requirements from ACI 318

## Slide 107: Beam Reinforcement: Layout
1
4
4
Notes: This figure presents layout of longitudinal reinforcement for Frame 1, in the elevation of beams between gridlines A and D.
The other beams can be checked in a similar manner.

## Slide 108: Determine Beam Design Shear
Probable moment
strength, Mpr (k-in)
Vu,grav = 34.1 kips
B
C
20’ – 30”
= 17’-6”=210”
7,929
6,841
Assumed
hinging
mechanism
Notes: The top right figure shows the hinging mechanism in which the maximum probable negative moment is developed at one end of the beam and the maximum probable positive moment is developed at the other end. The bottom left figure show the shear distribution between B and C.
Next we will determine the design shear forces for the beams. These shears are based on the illustrated hinging mechanism in which the maximum probable negative moment is developed at one end of the beam and the maximum probable positive moment is developed at the other end. The shears from the probable moments are then combined with the gravity shear to determine the total design shear.

## Slide 109: Beam Shear Force
Design shear
Factored
gravity shear
Seismic shear
Beam moments
Hinge locations
Notes: This figure shows the shear calculations, from defining the hinge locations, calculating beam moments, seismic shear and factored gravity shear, and finally the design shear by combining seismic and gravity shears.
The design shear is the gravity plus the seismic shear. Seismic shear is computed based on the flexural strength (Mpr) of the beams based on an assumed hinging pattern.

## Slide 110: Beam Reinforcement: Transverse
At ends of beam s = 6 in.
(near midspan, s = 6.0 in. w/ 2 legged stirrup)
Vseismic > 50% Vu therefore take Vc = 0
Use 4 legged #4 stirrups
Notes: This slide presents the calculation of the beam transverse reinforcement.
Note that Vc is taken as 0. #4 hoops are selected for the calculations, then the maximum spacing of hoops within the potential hinging region is determined as shown.

## Slide 111: Beam Reinforcement: Transverse
Check maximum spacing of hoops within plastic hinge length (2h)
  d/4 = 7.4 in.
  6db = 6.0 in.
  6 in.
  Therefore, 6.0 in. spacing at ends is adequate
  At beam rebar splices, s = 4.0 in.
Notes: This slide presents detailing of transverse reinforcement in the beam.
After calculating the required spacing to provide adequate shear strength, the spacing is checked against the maximum allowable spacing as shown in this slide. In this case the required spacing for shear strength governs.

## Slide 112: Joint Shear Force
But how to compute Vcol?
C
T
Vcol
Vj
Notes: This figure presents free body diagram at a beam-column joint.
The design shear for joints is determined from the maximum probable flexural capacities of the beams framing into the joint and the shear in the columns. In this way, the joint shear is directly related to the amount of reinforcement in the beams framing into the joints. But how is the column shear computed in this limit state analysis?

## Slide 113: Joint Shear Force
At 7th Floor, Column C:
Notes: The figure shows a free-body diagram and the probable moment strengths of the beams at the face of column
This slide presents a way of calculating the column shear.
The column shear can be computed using a free-body diagram and the probable moment strengths of the beams at the face of column.

## Slide 114: Joint Shear Force
108
411
237
282
Notes: This figure presents free body diagram at a beam-column joint.
This slide presents the calculation of shear demand and capacity at the joint.
Once the column shears are determined, the joint shear force and stress can be calculated as shown in this slide. The joint shear force is based on the same mechanism and moments shown on the previous slide. The joint area is the same as the column area (30 in. x 30 in.). The computed joint shear strength is then compared to the factored shear in the joint. If the joint shear strength were computed as less than the factored demand, the area of flexural steel, the beam depth, or the column size can be modified to remedy the problem.

## Slide 115: Frame 1 Column Design
30"
Level 7
Level 6
20'-0"
20'-0"
32"
32"
P
L
= 78 kips Includes
P
D
= 367 kips level 7
13'-0"
A
A'
B
Design column using standard P-M interaction curve
then:
Column:
Notes: The figure shows the floor plan at level 6 and level 7.
This slide presents column design example.
Finally, we will consider the design of a representative column, in this case the Frame 1 column on grid A’ just below the 7th floor. Recall that ACI considers a member to be a “column” where the factored axial demand exceeds 0.1Agf’c. The column design is based on a P-M analysis and the sum of the column moment capacities must exceed the beam moment capacities at each joint.

## Slide 116: Column Design Moments Design for strong column based on nominal beam moment strengths
Column moments (Level 7), assume uniform distribution top and bottom
Beam moments (Level 7)
A
A'
B
6,406
5,498
7,142
7,142
Notes: This figure shows the calculation of the column design moments from beam flexural capacities and strong column-weak beam rule.
This method assumes an inflection point at midheight of the column which is reasonable in most cases for regular frame layouts.

## Slide 117: Column Transverse Reinforcement
nl: number of longitudinal bars that are laterally supported by the corner of hoops or by seismic hooks
Notes: This slide presents requirements for column transverse reinforcement.
Next the necessary column transverse reinforcement to provide confinement of the concrete core is calculated. The equation on the slide that results in the larger amount of confining steel will govern.

## Slide 118: Column Transverse Reinforcement Maximum spacing is smallest of: h/4 = 30/4 = 7.5 in. 6db = 6*1.0 = 6.0 in. (#8 bars) so calculated as follows: for 12 #8 vertical bars and #4 hoops, hx = 8.33 in. and so = 5.72 in. Next, check confinement requirements……
Notes: This slide presents the rules to calculate maximum hoop spacing within the potential hinge region.

## Slide 119: Column Transverse Reinforcement Therefore, use #4 bar hoops with 4 legs Ash = 0.80 in2
Assume 4 in. hoop spacing:
fc' < 10,000 psi and Pu< 0.3fc'Ag Equation (c) was not required.
Notes: This slide presents design of column transverse reinforcement.
For most columns in Special moment frames, 4 inch hoop spacing is a reasonable assumption, so we start there.

## Slide 120: Determine Column Shear Based on probable moment strength of columns and can be limited by probable moment strength of beams
Mpr,2
Mpr,4
Mpr,1
Mpr,3
n
Mpr,top
Mpr,bottom
Vseismic
Vseismic
Notes: The figures shows the free-body diagram of a column and the shear stress distribution along the height.
The seismic shear in the columns can based on the probable flexural strength of the columns themselves or by the probably flexural strength of the beams that frame into the column at the top and the bottom.
Using the column moment strengths is conservative, but if the amount of shear reinforcement is governed by the confinement requirements, there may be adequate shear capacity for the conservative but more simple method.
If the probable moments in the beams are used, the column moments above and below the joint are determined based on their relative flexibilities. Then the shear in the column is calculated based on the moments at the top and the bottom of the column and the column clear height.

## Slide 121: Column Shear Design
Vc can be included in shear calculation
Based on column moments:
Mpr,col = 14,940 k-in (12 #8 vert and Pmax)
Notes: This slide presents calculation of column shear demend.
In this slide the shear demand in the column is calculated based on the column moment strengths.
Note that since there is significant axial compression in the column, concrete shear strength may be used.

## Slide 122: Column Shear Design Assume 6 in. max hoop spacing at mid-height of column
4 legs #4
s = 6 in. max
Hoops:
Notes: The figure shows hoops spaced at 6 inches in the middle of the column.
This slide shows the calculation of the concrete contribution to column shear strength.
Then the required shear strength to be provided by the steel is determined. The shear strength provided by the hoops spaced at 6 inches in the middle of the column (4 inch spacing is required spacing for confinement at the column ends) is shown to be more than adequate. Therefore, the final hoop layout within the plastic hinge lengths at the tops and bottoms of the columns is set.

## Slide 123: Column Reinforcement
Confinement length, lo, greater of:
  h = 30 in.
  Hc/6 = (156-32)/6 = 20.7 in.
  18 in.
  Therefore, use 30 in.
Notes: This figure shows the final column reinforcing layout.
Outside of the plastic hinge length, the spacing of the hoops can be increased to 6 inches.

## Slide 124: Intermediate Moment Frames
Beams
Columns
Notes: This slide presents design of intermediate moment frames.
Next, the design and detailing requirements for Intermediate moment frames are covered. While not addressed in this presentation, the Example Problems contains the detailed design of the example building as an intermediate moment frame as well as a special moment frame.

## Slide 125: Structural Wall Example
5 @ 20’ = 100’
7 @ 30’ = 210’
A
A’
B
C
C’
D
1
2
3
4
5
6
7
8
N
Typical Floor Plan
Same building as moment frame example
12-story concrete building
N-S direction: SMF
E-W direction: dual system
Seismic Design Category D
Modal Analysis Procedure
Shear wall @ grid 3-6
Notes: This figure presents a typical structural wall floor plan.
The same example problem used to illustrate the moment frame design will now be used to illustrate the concepts for Special structural walls. Recall that in the east-west direction, the building is a dual system with special moment frames on grids 1, 2, 7 and 8 and special structural walls on grids 3-6.

## Slide 126: Structural Wall
Shear wall cross section
Ag = (16)(210)+2(30)(30) = 5,160 sq in
Acv = 16[(210)+2(30)] = 4,320 sq in
16”
17’-6”=210”
30” x 30” column
Notes: This figure presents the geometry of the structural wall at gridline 3.
We will look at the wall at grid line 3 as shown in the left figure. The right side of the slide shows the plan section at the structural wall. The columns at the ends of the wall also serve as part of the north-south moment frame.

## Slide 127: Story Shears: E-W Loading
Notes: This figure presents the story shears on Frames Lines 1, 2, and 3.
This slide shows the story shears for East-West load application.
Note that Frame 3 includes the structural wall. Typical for cantilevered structural wall systems, the maximum shear and moment are at the base of the wall.

## Slide 128: Structural Wall Loading
At ground floor: shear and moment determined from the lateral analysis and axial load from gravity load run down.
All are factored forces.
Vu = 769 kips
Mu = 30,641 kip-ft
Pu,max = 6,044 kips
Pu,min = 2,460 kips
Notes: This slide provides the design loads at the base of the wall on grid 3.
The moment and shear come from the lateral analysis and gravity load comes from the load run-down and the worst case load combinations.

## Slide 129: Shear Panel Reinforcement
Vu = 769 kips (below level 2)
f’c = 5,000 psi, fy = 60 ksi
α = 2.0
 = 0.6 (per ACI 9.3.4(a))
Req’d rt = 0.0019
Min r (and rt) = 0.0025
Use #5 @ 12” o.c. each face:
rt= 0.0032 and Vn = 869 kips
Acv
rl
rt
Panel  to Acv
Notes: This shows the vertical and horizontal reinforcement in the structural wall.
First, the vertical and horizontal reinforcement required in the shear panel can be calculated.. The lower phi factor for structural wall shear is used because we will not provide enough shear reinforcement to enable the wall to develop it’s full flexural strength without a shear failure. This is permitted by the Provisions however, it is often preferable to ensure that the wall is flexure-controlled where practical. In some cases that is not practical.

## Slide 130: Axial-Flexural Design
At ground floor: shear and moment determined from the lateral analysis and axial load from gravity load run down.
All are factored forces.
Mu = 30,641 kip-ft
Pu,max = 6,044 kips
Pu,min = 2,460 kips
Notes: This slide presents axial-flexural design of the structural wall.
The axial and flexural (P-M) analysis is done using the loads provided previously.

## Slide 131: Axial and Flexural Design P-M interaction Wall reinforcement: #5 @12” o.c. Boundary reinforcement: 12 #9 each end
Notes: The figure shows the P-M interaction diagram.
This slide presents axial-flexural design of the structural wall. (Continued)
With the boundary column reinforcement assumed and the shear panel reinforcement selected, a column interaction curve can be generated and compared against the factored combinations of axial load and moment (using appropriate phi factors). In this case, the wall is more than adequate for the first two levels. The design could be further optimized to reduce boundary column reinforcing congestion, except that as noted previously, the column is part of the north-south moment frames.

## Slide 132: Boundary Element Check
Need confined boundary element
(extend up to below 9th floor where max stress < 0.15f’c)
Use stress-based procedure (ACI 18.10.6.3).
Boundary Elements required if max stress > 0.2f’c
Ground level axial load and moment are determined based on factored forces.
Notes: This slide presents the boundary element check for the structural wall.
We will check whether a boundary member is required based on the stress-based procedure of ACI 318. The axial load and moment come from the lateral and gravity load analysis of the building and the worst case load combination. The gross section properties are calculated, using the cross-section shown previously. Since a fairly large compressive stress is present, a boundary element is needed up thru the 8th floor.

## Slide 133: Boundary Element Length
Length = larger of c/2 or c-0.1Lw
From P-M interaction, max c = 72.6 in.
So, c/2 = 38.8 and c-0.1Lw = 50.6 in
Since length > column dimension, either
Extend boundary into wall panel
Increase f’c = reduce boundary element length
For this example, assume f’c = 7,000 psi,
Then req’d boundary element length is 28.7 in.
Notes: This slide illustrates the procedure for determining the extent of the boundary element confinement.
Since the length exceeds the column dimension, a higher strength concrete will be used in order to avoid having to confine the structural wall panel beyond the column.

## Slide 134: Boundary Element Confinement Transverse reinforcement in boundary elements is to be designed essentially like column transverse reinforcement. Assume #5 ties and 4 in. spacing
Width of the flexural compression zone, b > 12in. or hu/16
#5 with 4 legs, Ash = 1.24 in2
Notes: This figure presents design of transverse reinforcement for boundary element confinement.
The confinement is designed essentially like column confinement. For a hoop spacing of 4 in., 4 legs of #5 bar are required.

## Slide 135: Structural Wall Reinforcement
Notes: This slide shows a summary of the reinforcement for structural wall boundary members and panels.

## Slide 136: ACI 318, Overview of IMF: Beam Longitudinal Reinforcement
No specific splice req’ts
Joint face Mn+ not less than 33% Mn-
Min. Mn+ or Mn- not less than
20% max. Mn at joint face
Flexural reinforcement per Ch.9
Notes: This figure presents the beam longitudinal reinforcement requirements per ACI 318. The top figure shows the reinforcement ratio limits insure a tension controlled failure mode in bending and reduce congestion of reinforcing steel. Continuous bars in the top and bottom are required due to reversal of seismic motions and variable live load. The bottom two figures show that splice locations and transverse reinforcement are specified because lap splices are unreliable and cover concrete will spall.
This slide presents the beam longitudinal reinforcement requirements in an intermediate moment frame per ACI 318.
Continuous bars in the top and bottom are required due to reversal of seismic motions and variable live load. Unlike Special moment frames, there are no specific requirements for reinforcing ratios or for splices.

## Slide 137: ACI 318, Overview of IMF: Beam Transverse Reinforcement
Longitudinal bars on perimeter
tied as if column bars
Stirrups elsewhere, s  d/2
2h
min
Closed hoops at beam ends
Maximum spacing of hoops:
d/4 8db 24dbh 12”
Notes: The top figure show the hoop design requirements and the bottom figure shows the spacing requirement of hoops.
This slides presents transverse reinforcement requirements in an intermediate moment frame per ACI 318.
The hoop requirements for intermediate moment frame beams are similar to those of special moment frame beams.

## Slide 138: ACI 318, Overview of IMF: Beam Shear Strength
V1
V2
1.2D + 1.0L + 0.2S + 2.0E
Two options:
Similar to Special Moment Frames using nominal moment strengths instead of probable moment strengths.
Design load combinations with 2x earthquake shear
Notes: The figure shows a beam under factored distributed loads.
This slide presents two methods to calculate the required beam shear strength in an intermediate moment frame.
For beam shear strength, the method for special moment frames can be used. Or, the design shear can be based on the analysis using twice the earthquake shear in the load combinations.

## Slide 139: ACI 318, Overview of IMF: Column Transverse Reinforcement
ï
ï
ï
ï
þ
ï
ï
ï
ï
ý
ü
ï
ï
ï
ï
î
ï
ï
ï
ï
í
ì

"
12
hmin/2
8db
o
s
24dbh
ï
ï
ï
ï
þ
ï
ï
ï
ï
ý
ü
ï
ï
ï
ï
î
ï
ï
ï
ï
í
ì
³
"
18
6
height
clear
hmax
o
l
Hoops at both ends of column: spacing so over length lo
Outside length lo, transverse reinforcement per Ch. 10
Notes: This slide presents spacing requirements of transverse reinforcement in an intermediate moment frame.
The spacing of column hoops at the ends of intermediate frames is similar to that of special moment frames.

## Slide 140: ACI 318, Overview of IMF: Column Shear Strength
1.2D + 1.0L + 0.2S + W0E
Two options:
Similar to Special Moment Frames using nominal moment strengths instead of probable moment strengths.
Design load combinations with W0x earthquake shear
Notes: This slide presents two methods to calculate the required column shear strength in an intermediate moment frame.
For column shear strength, the method for special moment frames can be used (using nominal moment strengths instead of probable moment strength)s. Or, the design shear can be based on the analysis using Omega 0 times the earthquake shear in the load combinations.

## Slide 141: Summary of Seismic Detailing for Frames
Issue | Ordinary | Intermediate | Special
Hinge development and confinement |  | minor | full
Bar buckling |  | lesser | full
Member shear |  | lesser | full
Joint shear | minor | minor | full
Strong column |  |  | full
Rebar development | lesser | lesser | full
Load reversal | minor | lesser | full
Notes: This slide summarizes the differences in detailing requirements for the three types of moment frames.
Special moment frames require special attention to each of the performance objectives. Intermediate frames have less strict requirements on all counts. Ordinary frames have very few requirements beyond those of gravity frames designed using ACI 318. Note that the detailing to avoid rebar congestion is important in special moment frames (use scaled drawings of joints for this task).

## Slide 142: Questions
Notes: 508 note: Slide to prompt questions from participants.

## Slide 143: DISCLAIMER
NOTICE: Any opinions, findings, conclusions, or recommendations expressed in this publication do not necessarily reflect the views of the Federal Emergency Management Agency. Additionally, neither FEMA nor any of its employees make any warranty, expressed or implied, nor assume any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, product or process included in this publication.
The opinions expressed herein regarding the requirements of the NEHRP Recommended Seismic Provisions, the referenced standards, and the building codes are not to be used for design purposes. Rather the user should consult the jurisdiction’s building official who has the authority to render interpretation of the code.
Any modifications made to the file represent the presenters' opinion only.